## Slide 1
POPC (1-palmitoyl-2-oleoyl-sn-glycero-3-phosphatidyl choline
c
One-pot polymerization
4.5 Å
a
b
6.5 Å
3 Å
QM-optimized pore scaffolds of channel 3
QM-optimized pore
scaffolds of channel 4
QM-optimized pore
Scaffolds of channel 5
c
MD snapshot of channel 3
MD snapshot of channel 4

## Slide 2
Suggestion: Above are main data to present, so any other data not shown here in detail could be sent back to the supporting information?
3a-LA permeability
Water (Pw, cm2/s) : 3.3 x 10-6
Selectivity (Pw/Ps) : 1.56 x 108
Figure 2. Selective water permeation through foldamer-based polymeric artificial water channels. a, Chemical structures of lipid anchor (LA) modified artificial water channels. b, Representative stopped-flow light scattering traces of 3 and 3-LA reconstituted DOPC vesicles under the inwardly directed osmotic gradients. c, Single channel permeability of each channel structures before and after LA modification. d and e, Schematic illustrations of HPTS-based fluorescence assays for (d) cation (Na+ or K+) and (e) chloride (Cl-) and proton conduction through the channels. f, Stopped-flow fluorescence traces of 3-LA reconstituted DOPC vesicles encapsulating lucigenin dyes for sensing Cl- ion permeation. The reconstituted vesicles were exposed to inwardly directed Cl- concentration gradients to measure quantitative Cl- permeation rates through the membranes. g, Comparison of water-to-salt permselectivity of 3a-LA channels to the values of several representative water channels and current polymeric desalination membranes.
a
c
b
d
e
f
g
h

## Slide 3
225 mM NaCl
225 mM NaNO3
SPQ
Cl-
H+
c
15 breakers
Plus
20 water molecules
Proton wire breakers inside P26a
After running longer the permeabilities of the channels changed slightly,
3.61, 1.87, 0.08 water molecules per nanosecond for 3-LA, 4-LA, and 5-LA respectively. The permeability of aquaporin tetramer (divided by 4) is 1.18 water molecules per nanosecond.
Proton wire breakers
Proton wire breakers inside 4
Water chain as the proton wire
=
3
4
5
b
d
e
AQP1
3.6 x 109 H2O/s
1.9 x 109 H2O/s
1.2 x 109 H2O/s
8.0 x 107 H2O/s
c
f
Channel 4
Channel 3
a
3
4
3
4
Notes: For Grotthus mechanism for proton transport, the two end water molecules form only one H-bond with their neighboring water molecules, and all the other water molecules in the water chain serve as both H-bond donor and acceptor to form two H-bonds. That is, any such water donors its H-atom to form the first H-bond, and uses its O-atom to accept another water's H-atom to form the 2nd H-bond.
That is, a water molecule that does not fall within the above two categories mostly can be called proton wire breaker. There are at least three possibilities: those that do not form H-bond with water molecules (very unlikely), that form only one H-bond with surrounding water molecules, and that only use its two H-atoms (NOT O-atom) to form two H-bonds with surrounding water molecules.
Figure 1 compares the structure and dynamics of water molecules in P26a-b channels as a function of simulation time; (A) the number of permeated water molecules, (B) the total number of water molecules inside the channel, (C) the total number of H-bonds created by the water molecules counted inside the channel and (D) the total number of proton wire breakers among the water molecules inside the channel.

## Slide 4
a
b
Reflection
coefficient
Pf (KCl)
Pf (sucrose)
Channels
4d-LA
gA
1.03 ± 0.01
0.53 ± 0.02
1.06 ± 0.01
0.07 ± 0.001
Pf (NaCl)
Pf (sucrose)
pH = 7.0
300 mM Sucrose
or 150 mM NaCl
or 150 mM KCl
pH = 7.0
H2O

## Slide 5
225 mM NaCl
SPQ
H+
a
pH = 7.0
200 mM Na2SO4
or K2SO4
pH = 7.0
HPTS
M+
H+
pH = 8.0
67 mM Na2SO4
pH = 7.0
100 mM NaCl
HPTS
Na+
H+
Cl-
or
OH-
or
225 mM NaNO3
Cl-
b
c
Notes: gramicidin A that has an estimated conductance of 1.1 x 10-17 A (one ampere of current = 6.242 × 1018 electrons) at pH 7.
Akeson, M.; Deamer, D. W. Proton conductance by the gramicidin water wire. Model for proton conductance in the F1F0 ATPases? Biophys. J. 1991, 60, 101-109;
For Grotthus mechanism for proton transport, the two end water molecules form only one H-bond with their neighboring water molecules, and all the other water molecules in the water chain serve as both H-bond donor and acceptor to form two H-bonds. That is, any such water donors its H-atom to form the first H-bond, and uses its O-atom to accept another water's H-atom to form the 2nd H-bond.
That is, a water molecule that does not fall within the above two categories mostly can be called proton wire breaker. There are at least three possibilities: those that do not form H-bond with water molecules (very unlikely), that form only one H-bond with surrounding water molecules, and that only use its two H-atoms (NOT O-atom) to form two H-bonds with surrounding water molecules.
Figure 1 compares the structure and dynamics of water molecules in P26a-b channels as a function of simulation time; (A) the number of permeated water molecules, (B) the total number of water molecules inside the channel, (C) the total number of H-bonds created by the water molecules counted inside the channel and (D) the total number of proton wire breakers among the water molecules inside the channel.

## Slide 6
EYPC-LUVs (without any dye) was used for this experiment.
a
b
d
c
e
f