Supplementary Information

Interplay between geological materials and the environment at the Dazu Rock Carvings, China

Haiqing Yang a, Xingyue Li a*, Francesca Cappitelli b

Author affiliations

a School of Civil Engineering, Chongqing University, Chongqing, China

b Department of Food, Environmental and Nutritional Sciences, Università degli Studi di Milano, via L. Mangiagalli 25, 20133, Milan, Italy

Corresponding authors: Xingyue Li (lixingyue@stu.cqu.edu.cn); ORCID: 0000-0003-1058-5228

First author: Haiqing Yang (yanghaiqing@cqu.edu.cn); ORCID: 0000-0003-4497-044X

Third author: Francesca Cappitelli (francesca.cappitelli@unimi.it); ORCID: 0000-0003-1237-1813

This file includes:

Supplementary Tables 1-3

Supplementary Figures 1-7

Supplementary Tables

Supplementary Table 1 EDS energy spectrum data of Dazu Rock Carvings sandstone (mass fraction, %)

|  | O | Si | C | Al | Fe | K | Mg | Ca | Cl | Na | Ti |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Internal cement | 33.3 | 13.1 | 36.5 | 7 | 4.1 | 2 | 2.1 | 0.7 | 0.8 | 0.4 | 0.2 |
| Mineral film | 34.8 | 21.2 | 19.9 | 10.2 | 6.7 | 4.0 | 1.9 | 0.6 | 0.3 | 0.3 | 0.3 |

Supplementary Table 2 Structural parameters of different samples extracted from the EXAFS fitting

| Sample | Shell | CN | R (Å) | σ2 (10-3Å2) | ΔE0 (eV) | R factor |
| --- | --- | --- | --- | --- | --- | --- |
| Fe foil | Fe-Fe | 12(fixed) | 2.49±0.01 | 4.1±1.6 | 3.1±5.2 | 0.002 |
| FeO | Fe-O | 5.8±0.5 | 2.17±0.01 | 5.2±2.8 | -1.9±4.2 | 0.01 |
|  | Fe-Fe | 11.3±0.9 | 3.06±0.01 | 2.1±1.8 | 2.3±3.7 |  |
| Fe2O3 | Fe-O | 2.8±0.3 | 2.01±0.01 | 3.7±1.9 | -3.6±5.7 | 0.014 |
|  | Fe-Fe | 11.5±0.9 | 2.98±0.01 |  |  |  |
| Mineral film | Fe-O | 3.5±0.2 | 2.18±0.01 | 3.1±2.3 | 0.7±3.1 | 0.017 |
|  | Fe-Fe | 9.7±0.3 | 3.07±0.01 | 1.7±0.9 | 6.2±6.4 |  |

Data ranges: 3.0 ≤ k ≤ 12.0 Å-1, 1.0 ≤ R ≤ 3.0 Å. R: bond distance; σ2: Debye-Waller factors; R factor: goodness of fit. S02 is the amplitude reduction factor (S02 =0.82 was obtained by Fe foil fitting and applied for the other samples fitting);

Supplementary Table 3 Concentration of C2O42- in the mineral film (IC)

| Ion | Concentration (mg/Kg) |
| --- | --- |
| C2O42- | 3.30 |

Supplementary Figures

Fig. S1. Morphology of the exposed surface at different scales. a, location of the Daza rock carvings in the Chongqing Municipality. b, Top view image of sandstone, the rectangular area is where a sample was taken. c, SEM image showing microscopic morphology of the exposed surface of sandstone (5000x). d-e, EDS analyses of sandstone point 1 and point 2 of the same sample.

Fig. S2. Morphology of the collected samples. a, location of sandstone sampling. b-c, The exposed and inner surfaces of sandstone samples. d-e, Microscopic morphology of the exposed surface and the inner surface of sandstone (2000x).

Fig. S3. Polarized images of three of the samples (mineral film). a-c, The first sample. d, The second sample. e, The third sample.

Fig. S4. Cumulative porosity of internal structure and mineral film. The results are obtained by binary processing of SEM image. Among them, the porosity of mineral membrane is 3.30%, and the porosity of internal structure is 12.57%.

Fig. S5. Mineral composition of Dazu Rock Carving Sandstone.

Fig. S6. Fe K-edge X-ray absorption near-edge structure (XANES) spectra of mineral layers. a, XANES spectra. b, Radial structure functions. c-f, Wavelet transform for Fe foil, FeO, Fe2O3, and mineral film. Fe foil, FeO and Fe2O3 were used as reference materials the measurements.

Fig. S6. Superimposed curves of experimental results for the samples of mineral film compared with different standard compounds. a, EXAFS functions. b, Fourier Transforms.

Fig. S7. Organic carbon content of mineral film. TC, EC, and OC represents total carbon, elemental carbon, and organic carbon, respectively.

Fig. S8. Pearson correlation coefficients among selected elemental attributes.