Supporting Information

Tailoring Friction control in 3D Printed Patterned Multi-Materials: A Flexible Design Strategy

Xinle Yao a,b, Yuxiong Guo b,c, Mingyang Wang a,b, Yaozhong Lu b,c, Zhibin Lu b, Xin Jia a,*, Yu Gao b,*, Xiaolong Wang b,*

a School of Chemistry and Chemical Engineering, Key Laboratory of Materials-Oriented Chemical Engineering of Xinjiang Uygur Autonomous Region, Shihezi University, Shihezi, China

b State Key Laboratory of Solid Lubrication, Lanzhou Institute of Chemical Physics, Chinese Academy of Sciences, Lanzhou, China

c Shandong Laboratory of Advanced Materials and Green Manufacturing at Yantai, Yantai 264006, China

*Corresponding authors: Xin Jia, E-mail: jiaxin@shzu.edu.cn; Yu Gao, E-mail: gaoyu@licp.cas.cn; Xiaolong Wang, E-mail: wangxl@licp.cas.cn;

Table S1 Mean friction coefficient of Muti- material composites

Fig. S1 Wear tracks and tribo-film of PI-Gr composites.

Fig. S2 The printed samples of (a)PI, (b)PI-PTFE and (c)PI-Gr.

Fig. S3 Densities of PI, PI-PTFE and PI-Gr composites.

Fig. S4 Wear tracks and tribo-film of PI, PI-PTFE and PI-Gr composites.

Table S2 Thermal, mechanical and tribological properties of PSPI and PSPI-PTFE composites

| Code | Density (g/ml) | Hardness (GPa) | Modulus (GPa) | COF | WR (×10-5mm3/N∙m) |  |
| --- | --- | --- | --- | --- | --- | --- |
| PI | 1.44 | 6.02 | 0.38 | 0.65 |  | 22.47 |
| PI-PTFE | 1.45 | 5.36 | 0.29 | 0.04 |  | 0.04 |
| PI-Gr | 1.45 | 5.97 | 0.35 | 0.26 |  | 0.23 |

Fig. S5 The printed dual-material samples of (a)PI/PI-PTFE, (b)PI/PI-Gr and (c)PI-Gr/PI-PTFE.

Fig. S6 Wear tracks and tribo-film of (a)PI/PI-PTFE, (b)PI/PI-Gr and (c)PI-Gr/PI-PTFE.

Figure S7. Pearson’s correlation heatmap between features for database II.

Figure S8. Comparison of experimental values and ML prediction values using LR algorithm for database II.

Figure S9. Scatter plot matrix of features and calculation of COF values in the range 0.48-0.67. (a) The importance of PI and PI.4, (b) the importance of PI, PI-Gr.4, and PI.16.

Figure S10. Scatter plot matrix of features and calculation of COF values in the range 0.31-0.48. (a) The importance of PI, PI-Gr.4 and PI.16, (b) the importance of PI and PI-PTFE.4, (c) the importance of PI-PTFE, PI.4, and PI.16.

Figure S11. Scatter plot matrix of features and calculation of COF values in the range 0.17-0.31. (a) The importance of PI-PTFE, PI.4 and PI.16, (b) the importance of PI-PTFE, PI.4, and PI.16.

Figure S12. Scatter plot matrix of features and calculation of COF values in the range 0-0.17.

Table. S3 Formulation of the PI, PI-PTFE and PI-Gr composites.

| Code | PI Powder (%) | NVP (%) | TMPTA (%) | DMF a (%) | 819 b (%) | PTFE Micropowder c (%) | Gr Micropowder d (%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| PI | 60 | 30 | 10 | 16 | 2 | - | - |
| PI-PTFE | 60 | 30 | 10 | 16 | 2 | 10 | - |
| PI-Gr | 60 | 30 | 10 | 16 | 2 | - | 1, 2, 3, 4 |

Note: a, b, c, and d represents the amount added as a percentage of the total ink mass