Supplementary File

| Ion Extended model | Temperature | AICC Δi Wi |
| --- | --- | --- |
|  | 298 | 303 313 | 298 303 313 298 303 313 298 303 313 |
| Cs+ | Langmiur Freundlish R-P | Q0,mg/g b, l/mg RL Kf,mg/g n KR, l/mg α b | 188.23 0.015 0.0426 4.19 1.37 2.35 0.005 0.999 | 197.7 0.018 0.035 55.56 1.41 2.36 0.006 0.999 | 211.71 0.011 0.0571 58.02 1.99 2.37 0.007 0.999 | -10.88 104.34 -90.256 111.42 129.87 114.00 -123.52 68.70 -380.35 | -10.89 35.63 290.09 234.94 61.16 494.35 0 0 | 0.995 1.84E-8 1.01E-63 4.14E-54 5.23E-14 4.49E-108 0.004 0.999 1 |
| Sr2+ Langmiur Freundlish R-P | Q0,mg/g b, l/mg RL Kf,mg/g n KR, l/mg α b | 152.77 155.81 169.44 0.008 0.008 0.001 0.0769 0.0769 0.0204 2.52 48.95 51.72 1.34 1.37 1.92 1.78 1.89 2.08 0.003 0.006 0.007 1.096 1.24 1.25 | -35.12 43.04 -102.77 99.37 105.48 110.62 76.84 -30.17 | 0 0 0 134.49 62.43 213.38 125.43 33.69 72.59 | 1 1 1 6.23E-30 2.78E-14 4.61E-47 5.788E-28 4.83E-8 1.72E-16 |

Table S1. The calculated parameters of Langmiur; Freundlish and R-P isotherm models for Cs+ and Sr2+ sorbed onto the prepared material at different temperatures

Table S2. Physico-chemical properties of Cs+ and Sr2+

| Characteristics of ions | Cs+ | Sr2+ |
| --- | --- | --- |
| Atomic Weight | 132.91 | 87.62 |
| Ionic radius r(pm) | 167 | 112 |
| Electronegativity (Pauling) , Xm | 0.79 | 0.95 |
| Covalent index , Xm2r-1 | 1.042 | 0.805 |
| Ionic index, z2r-1 | 0.598 | 3.57 |

Fig.S1. Linear plot of lnk2 versus 1/T.

Fig.S2. Comparison between experimental and predicted data obtained using the extended Langmuir; Freundlish and R-P model.