Supporting Information

Three pure inorganic materials based on Strandberg-type phosphomolybdate and different transition metal linkers

CHUNXIAO WANG, JIE SHI, KAI YU* and BAIBIN ZHOU*

1. Structural figures

Figure S1. ORTEP view of the basic units of 1 with 50% thermal ellipsoids.

Figure S2. ORTEP view of the basic units of 2 with 50% thermal ellipsoids.

Figure S3. ORTEP view of the basic units of 3 with 50% thermal ellipsoids.

Figure S4. Polyhedral and ball–stick representation of supramolecular (a) 1-D chains and (b) 2-D layers of 3 extended by hydrogen bonds and supramolecular interactions.

Figure S5. Polyhedral representation of supramolecular 3-D networks of 2 extended by hydrogen bonds and supramolecular interactions.

Figure S6 Polyhedral representation of supramolecular 3-D networks of 3 extended by hydrogen bonds and supramolecular interactions.

2. Structural data

Table S1. Selected bond lengths (Å) of 1-3.

| Compound 1 |
| --- |
| Mo(1)-O(7) | 2.312(15) | Mo(2)-O(6) | 1.916(15) |
| Mo(1)-O(7)#5 | 2.312(15) | Mo(2)-O(7)#5 | 2.341(16) |
| Mo(1)-O(10) | 1.901(9) | Mo(2)-O(8) | 2.201(15) |
| Mo(1)-O(10)#5 | 1.901(8) | Mo(2)-O(10) | 1.972(9) |
| Mo(1)-O(13) | 1.718(10) | Mo(2)-O(14) | 1.722(10) |
| Mo(1)-O(13)#5 | 1.718(10) | Mo(2)-O(16) | 1.718(10) |
| Mo(3)-O(6) | 1.935(15) | Ag(1)-O(10) | 2.473(8) |
| Mo(3)-O(8) | 2.342(15) | Ag(1)-O(17) | 2.265(9) |
| Mo(3)-O(9) | 1.910(6) | Ag(1)-O(10)#6 | 2.473(8) |
| Mo(3)-O(11)#5 | 2.265(8) | Ag(1)-O(17)#6 | 2.265(9) |
| Mo(3)-O(12) | 1.708(9) | P(1)-O(7) | 1.553(16) |
| Mo(3)-O(15) | 1.723(10) | P(1)-O(8) | 1.562(15) |
| Mo(3)#5-O(9) | 1.910(6) | P(1)-O(11) | 1.531(9) |
| P(1)-O(17) | 1.522(9) |  |  |
| O(7)#5-Mo(1)-O(7) | 79.8(8) | O(6)-Mo(2)-O(7)#5 | 89.3(6) |
| O(10)-Mo(1)-O(7) | 82.3(5) | O(8)-Mo(2)-O(7)#5 | 72.4(5) |
| O(10)#5-Mo(1)-O(7) | 73.3(5) | O(10)-Mo(2)-O(7)#5 | 71.4(4) |
| O(13)-Mo(1)-O(7) | 88.0(5) | O(14)-Mo(2)-O(7)#5 | 89.5(5) |
| O(13)#5-Mo(1)-O(7) | 166.1(6) | O(16)-Mo(2)-O(7)#5 | 160.8(5) |
| O(6)-Mo(3)-O(8) | 70.5(6) | O(10)-Ag(1)-O(10)#6 | 179.999(1) |
| O(9)-Mo(3)-O(8) | 84.1(6) | O(17)-Ag(1)-O(10)#6 | 92.0(3) |
| O(11)#5-Mo(3)-O(8) | 86.4(4) | O(17)#6-Ag(1)-O(10)#6 | 88.0(3) |
| O(12)-Mo(3)-O(8) | 169.9(5) | O(7)-P(1)-O(8) | 108.7(8) |
| O(15)-Mo(3)-O(8) | 85.3(5) | O(11)-P(1)-O(8) | 106.3(7) |
| O(17)-P(1)-O(8) | 109.5(7) |  |  |
| Compound 2 |
| P(1)-O(3) | 1.567(10) | P(2)-O(4) | 1.53(2) |
| P(1)-O(5) | 1.521(10) | P(2)-O(7) | 1.576(10) |
| P(1)-O(6) | 1.562(10) | P(2)-O(8) | 1.52(2) |
| P(1)-O(12) | 1.516(9) | P(2)-O(16) | 1.532(10) |
| Mo(1)-O(4) | 2.32(2) | Mo(2)-O(2) | 1.950(10) |
| Mo(1)-O(6) | 2.361(9) | Mo(2)-O(5) | 2.259(10) |
| Mo(1)-O(9) | 1.910(10) | Mo(2)-O(13) | 1.894(10) |
| Mo(1)-O(11) | 1.925(10) | Mo(2)-O(16) | 2.400(9) |
| Mo(1)-O(15) | 1.697(11) | Mo(2)-O(23) | 1.714(11) |
| Mo(1)-O(18) | 1.717(11) | Mo(2) )-O(27) | 1.697(11) |
| Mo(3)-O(2) | 1.918(10) | Mo(4)-O(3) | 2.314(9) |
| Mo(3)-O(6) | 2.321(9) | Mo(4)-O(8) | 2.36(2) |
| Mo(3)-O(9) | 1.951(10) | Mo(4)-O(10) | 1.700(11) |
| Mo(3)-O(16) | 2.228(9) | Mo(4)-O(13) | 1.899(10) |
| Mo(3)-O(17) | 1.704(11) | Mo(4)-O(14) | 1.947(10) |
| Mo(3)-O(22) | 1.722(11) | Mo(4)-O(21) | 1.714(11) |
| Mo(5)-O(3) | 2.165(9) | Cu(1)-O(12) | 2.024(9) |
| Mo(5)-O(4) | 2.44(2) | Cu(1)-O(12)#4 | 2.024(9) |
| Mo(5)-O(11) | 1.932(10) | Cu(1)-O(19) | 2.160(11) |
| Mo(5)-O(14) | 1.922(10) | Cu(1)-O(19)#4 | 2.160(11) |
| Mo(5)-O(25) | 1.702(12) | Cu(1)-O(20) | 2.123(10) |
| Mo(5)-O(26) | 1.731(12) | Cu(1)-O(20)#4 | 2.123(10) |
| O(12)-P(1)-O(3) | 108.8(6) | O(8)-P(2)-O(4) | 112.1(12) |
| O(12)-P(1)-O(5) | 111.9(6) | O(8)-P(2)-O(7) | 109.9(9) |
| O(12)-P(1)-O(6) | 110.8(5) | O(8)-P(2)-O(16) | 109.1(10) |
| O(15)-Mo(1)-O(4) | 169.5(7) | O(27)-Mo(2)-O(2) | 101.0(5) |
| O(15)-Mo(1)-O(6) | 89.2(4) | O(27)-Mo(2)-O(5) | 84.2(5) |
| O(15)-Mo(1)-O(9) | 101.1(5) | O(27)-Mo(2)-O(13) | 102.9(5) |
| O(15)-Mo(1)-O(11) | 99.5(5) | O(27)-Mo(2)-O(16) | 167.8(4) |
| O(15)-Mo(1)-O(18) | 104.2(5) | O(27)-Mo(2)-O(23) | 103.4(6) |
| O(17)-Mo(3)-O(2) | 99.4(5) | O(10)-Mo(4)-O(3) | 164.6(5) |
| O(17)-Mo(3)-O(6) | 164.8(5) | O(10)-Mo(4)-O(8) | 83.4(7) |
| O(17)-Mo(3)-O(9) | 94.3(5) | O(10)-Mo(4)-O(13) | 104.3(5) |
| O(17)-Mo(3)-O(16) | 96.6(5) | O(10)-Mo(4)-O(14) | 97.6(5) |
| O(17)-Mo(3)-O(22) | 105.1(6) | O(10)-Mo(4)-O(21) | 102.5(5) |
| O(25)-Mo(5)-O(3) | 99.1(5) | O(12)-Cu(1)-O(12)#4 | 179.999(3) |
| O(25)-Mo(5)-O(4) | 166.2(7) | O(12)-Cu(1)-O(19) | 93.0(4) |
| O(25)-Mo(5)-O(11) | 97.2(5) | O(12)-Cu(1)-O(19)#4 | 87.0(4) |
| O(25)-Mo(5)-O(14) | 100.5(5) | O(12)-Cu(1)-O(20) | 93.6(4) |
| O(25)-Mo(5)-O(26) | 104.6(7) | O(12)-Cu(1)-O(20)#4 | 86.4(4) |
| Compound 3 |
| O(5)-P(1) | 1.565(7) | O(1)-P(2) | 1.576(8) |
| O(9)-P(1) | 1.564(8) | O(6)-P(2) | 1.533(8) |
| O(10)-P(1) | 1.523(8) | O(8)-P(2) | 1.520(8) |
| O(13)-P(1) | 1.510(8) | O(15)-P(2) | 1.535(8) |
| O(6)-Mo(1) | 2.325(7) | O(20)-Mo(2) | 1.718(8) |
| O(4)-Mo(1) | 1.910(8) | O(19)-Mo(2) | 1.692(8) |
| O(5)-Mo(1) | 2.366(7) | O(15)-Mo(2) | 2.399(7) |
| O(7)-Mo(1) | 1.926(8) | O(2)-Mo(2) | 1.899(8) |
| O(12)-Mo(1) | 1.701(8) | O(10)-Mo(2) | 2.257(7) |
| O(11)-Mo(1) | 1.717(8) | O(3)-Mo(2) | 1.956(7) |
| O(3)-Mo(3) | 1.920(8) | O(17)-Mo(4) | 1.713(8) |
| O(4)-Mo(3) | 1.951(7) | O(18)-Mo(4) | 1.951(8) |
| O(5)-Mo(3) | 2.313(7) | O(16)-Mo(4) | 1.708(8) |
| O(15)-Mo(3) | 2.227(7) | O(2)-Mo(4) | 1.893(8) |
| O(14)-Mo(3) | 1.711(8) | O(8)-Mo(4) | 2.359(7) |
| O(23)-Mo(3) | 1.707(9) | O(9)-Mo(4) | 2.321(7) |
| O(21)-Mo(5) | 1.715(9) | Co(6)-O(24) | 2.127(8) |
| O(22)-Mo(5) | 1.711(10) | Co(6)-O(25) | 2.167(8) |
| O(18)-Mo(5) | 1.922(8) | Co(6)-O(13)#1 | 2.029(7) |
| O(7)-Mo(5) | 1.936(7) | Co(6)-O(24)#1 | 2.127(8) |
| O(9)-Mo(5) | 2.163(7) | Co(6)-O(25)#1 | 2.167(8) |
| O(6)-Mo(5) | 2.429(8) | Co(6)- O(13) | 2.029(7) |
| O(12)-Mo(1)-O(11) | 104.1(4) | O(12)-Mo(1)-O(7) | 99.2(4) |
| O(12)-Mo(1)-O(4) | 101.2(4) | O(12)-Mo(1)-O(6) | 169.2(3) |
| O(19)-Mo(2)-O(20) | 103.0(4) | O(12)-Mo(1)-O(5) | 89.4(3) |
| O(19)-Mo(2)-O(3) | 100.9(4) | O(19)-Mo(2)-O(2) | 103.1(4) |
| O(19)-Mo(2)-O(15) | 168.0(3) | O(19)-Mo(2)-O(10) | 84.5(4) |
| O(23)-Mo(3)-O(3) | 99.0(4) | O(23)-Mo(3)-O(14) | 104.8(4) |
| O(23)-Mo(3)-O(15) | 158.1(4) | O(23)-Mo(3)-O(4) | 100.4(4) |
| O(16)-Mo(4)-O(17) | 102.6(4) | O(23)-Mo(3)-O(5) | 85.4(3) |
| O(16)-Mo(4)-O(2) | 104.2(4) | O(16)-Mo(4)-O(18) | 97.9(4) |
| O(16)-Mo(4)-O(8) | 83.4(4) | O(16)-Mo(4)-O(9) | 164.7(4) |
| O(22)-Mo(5)-O(18) | 100.8(4) | O(22)-Mo(5)-O(21) | 104.3(5) |
| O(22)-Mo(5)-O(9) | 99.0(4) | O(22)-Mo(5)-O(7) | 96.8(4) |
| O(13)-P(1)-O(10) | 112.0(5) | O(22)-Mo(5)-O(6) | 165.9(4) |
| O(13)-P(1)-O(9) | 108.7(4) | O(8)-P(2)-O(6) | 111.6(5) |
| O(13)-P(1)-O(5) | 111.1(4) | O(8)-P(2)-O(15) | 108.9(4) |
| O(13)#1-Co(6)-O(25)#1 | 92.7(3) | O(8)-P(2)-O(1) | 110.2(4) |
| O(13)-Co(6)-O(25)#1 | 87.3(3) | O(24)-Co(6)-O(25)#1 | 91.5(4) |
| O(25)-Co(6)-O(25)#1 | 179.999(1) | O(24)#1-Co(6)-O(25)#1 | 88.5(4) |

3. Physical characterization

Figure S7. IR spectra of (a) 1, (b) 2, and 3.

Figure S8. TG curves of (a) 1, (b) 2, and 3.

Figure S9. XRD powder patterns of (a) 1, (b) 2, and 3.

Figure S10. The cyclic voltammograms of (a) 1-CPE, (b) 2-CPE, and (c) 3-CPE in 0.5 mol·L-1 H2SO4 aqueous solutions at different concentrations (from inner to outer: 20, 40, 60, 80, 100, 120, 150, 180, 210, and 240 mV·s-1 for 1-CPE; 20, 40, 60, 80, 100, 120, 140, and 160 mV·s-1 for 2-CPE; 20, 40, 60, 80, 100, 120, and 140 mV·s-1 for 3-CPE)