## Slide 1: Investigating the difference in nucleation during Si-based ALD on different surfaces (Si, SiC, SiO2 and SiNx) for future area-selective deposition (AS-ALD)
24.07.2018
E. A. Filatova*a, A. Mamelib, A. J. M. Mackusb, F. Roozeboomb,
W.M.M. Kesselsb, D. Hausmannc, S.D. Elliotta,d
a Tyndall National Institute, University College Cork, Ireland
b Eindhoven University of Technology, The Netherlands
c Lam Research Corporation, USA
d currently at Schrödinger Inc, Ireland
Notes: Please use the title from the abstract

## Slide 2
Microchip
Deposition of materials on high-aspect-ratio surfaces
source: Fundamentals of Semiconductor Devices, 2004, Betty Anderson, Richard Anderson

## Slide 3
Atomic layer deposition (ALD)
precursor A
precursor B
purge
+ by-products
Low temperature
Conformal
on high-aspect-ratio surfaces
Precise thickness control
+ by-products

## Slide 4
Conventional lateral dimension control Lithography
Resist film patterned
by lithography
Removal of excess material using etching
Misalignment error!
4
Notes: Something seems to be missing here. I don’t see a misalignment error in the figure.

## Slide 5
Alternative: self-aligned fabrication
area-selective ALD
Different surface chemistry
5
Notes: You can refer here to self-aligned fabrication.

## Slide 6
Theoretical modelling
for area-selective deposition
ΔE
> 0 thermodynamically unfavorable
< 0 thermodynamically favorable
6
DFT:
Notes: Alfredo: Great! What about kinetics? Maybe you can also mention that in words

## Slide 7: Theory: DFT Adsorption of Si precursor and elimination of one ligand
ΔE = E (slab + precursor) + E (by-products) – E (slab) – E (precursor)
8
VASP software
before reaction
after reaction

## Slide 8: Goal: investigating the difference in nucleation during Si-based ALD for future area-selective deposition for electronic devices
Si3N4
SiO2
Excellent barrier
Low-k
Low wet etch rate
SiC
Si
2
Notes: About which material is the description at the right?

## Slide 9
Si-based thin films for electronic devices: Applications
Low-k spacers/liners
Air gap liners for interlayer dielectric
3
Notes: The reference is missing

## Slide 10
Investigating area-selective ALD
of Si-based materials
α-quartz-SiO2:OH
(0 0 1) 1X2
β-3C-SiC:H
Si:H
(0 1 1)
(0 0 1)
Precursors:
DSBAS
Surfaces:
DIPAS
BTBAS
SiCl4
SiBr4
7
“Slab” – surface model (periodic in x and y, vacuum in z)
Side view
Aminosilanes
Halides

## Slide 11: DFT results First precursor adsorption step
Precursors | ΔE, eV |  | 
 | Si:H | SiC:H | SiO2:OH
DIPAS | 0.10 | 0.49 | -0.19
DSBAS | 0.08 | 0.46 | -0.21
BDEAS | -0.01 | 1.04 | -0.18
SiCl4 | 0.64 | 1.17 | 0.35
SiBr4 | 0.58 | 1.12 | 0.28
BDEAS
DIPAS
DSBAS
at T = 0 K
Aminosilane precursors:
Halide precursors:
9
SiO2
SiC
Si
SiO2
SiC
Si

## Slide 12
ALD experiment SiNx PEALD
Dr. Alfredo Mameli
Precursor: DSBAS
N2 plasma
150 OC
Flexal system, Oxford Instruments
Notes: Flexal system from Oxford Instruments which is equipped with a turbo pump a load-lock 300 mm surstrate table and ICP plasma source

## Slide 13
ALD experiment SiNx PEALD
HF last c – Si:H
(HF 4 min on Si wafer)
c - Si:OH
(native oxide on Si wafer)
α-quartz-SiO2:OH
(0 0 1) 1X2
β-3C-SiC:H
Si:H
(0 1 1)
(0 0 1)
Surfaces:
H2 plasma
SiC wafer
10
Notes: You should mention a bit more about the experimental details (e.g. refer to the use of ellipsometry, etc.). Please let me know if you need specific figures.

## Slide 14
1 DSBAS dose
Spectroscopy ellipsometry (SE)
every half cycle
2 DSBAS dose
3 DSBAS dose
(SE)
(SE)
(SE)
N2 plasma dose
(SE)

## Slide 15
ALD experiment SiNx PEALD
SE every half cycle
First DSBAS adsorption step:
ΔE:
0.08 eV
-0.21 eV
0.46 eV
N2 plasma modifies Si:H and SiC:H surface to SiNx,
allowing the growth on all of the surfaces
Selectivity
DFT predicts results right
12
SiO2
SiC
Si
Notes: Especially this slide requires more explanation about how it is measured…
Please change ‘SiN thickness’ to ‘Apparent thickness’. After just dosing the precursor, it’s not SiN yet.
Including the reference data is confusing, since it should be a straight line if you measure after every SE halfcycle.
Alfredo: the reference is SiNx thickness grown on similar substrates after 5 cycles. The SiNx layers were grown for 200 cycles and measured in situ every 5 cycles. The thickness after the first 5 cycles is taken as a reference and to model the half-cycles data. But I agree that it can be confusing to the scope of the ppt. (so removed)
I sent you some literature on N2 plasma modification of Si surfaces, you can maybe cite one of those papers.

## Slide 16
Conclusions
DFT predicts the experiment right
N2 plasma modifies Si and SiC surface to SiNx,
allowing the growth on all of the surfaces
13
None of halide precursors SiCl4, SiBr4 adsorb on Si-based surfaces at 0K
Selectivity! Aminosilane precursor DSBAS adsorbs selectively on SiO2 and Si3N4 not on Si and SiC
Notes: It would be good to also refer to the modelling results for the other precursors here.
“Selective growth” should be “Selective adsorption”.
Si:H and SiO2 instead of Si:H twice

## Slide 17
Acknowledgements

## Slide 18: Ekaterina Filatova Email: ekaterina.filatova@tyndall.ie
Theoretical modelling of area-selective atomic layer deposition (AS-ALD) Si-based materials
Notes: Please use the title from the abstract