## Slide 2: Exploring doping in bulk chromia: Effects of dopant oxidation state on composition, vacancy defects and vacancy migration
John J. Carey and Michael Nolan
Tyndall National Institute, University College Cork, Cork, Ireland
michael.nolan@tyndall.ie

## Slide 3
Chromium oxide is a reducible oxide with oxidation states from Cr(II) to Cr(VI)
Crystallises in different phases: CrO, Cr2O3, Cr2O5, and CrO3
Hexagonal corundum structure (α-Cr2O3) the most thermodynamically stable at low temperatures and pressures.
Introduction
Dielectric material with wide band gap ~ 3eV
Valence band maximum (VBM) and conduction band minimum (CBM) are a mix of Cr 3d states and O 2p states
Anti-ferromagnetic material with alternating “-+-+” Cr layers

## Slide 4
While not as widely used as TiO2 or CeO2 chromia finds many applications
Oxygenation catalysis, methanol synthesis, anode material for Li-ion batteries, gas sensors, solid oxide fuel cells, protective coatings, adhesion promotors
Defect formation key to properties
p-type TCO materials: Mg/Ni:Cr2O3 – important role of defects in promoting TCO characteristics
Introduction
Dielectric material with wide band gap ~ 3eV
Valence band maximum (VBM) and conduction band minimum (CBM) are a mix of Cr 3d states and O 2p states
Anti-ferromagnetic material with alternating “-+-+” Cr layers
O vacancy formation – 4.11 eV
Cr vacancy – 4.59 eV

## Slide 5
p-type TCO materials: Mg/Ni:Cr2O3 – important role of defects in promoting TCO characteristics
Example of p-type Doping
Comparison between the Arrhenius plot of a Ni-doped (red triangles) and a Mg-doped (blue diamonds) Cr2O3 thin films.
Conductivity of Ni-doped Cr2O3 prepared with 7% Ni function of deposition temperature
Ni doping introduces new states near VB edge which contributes to hole localisation
p-type defects favourable to form and under growth conditions not compensated

## Slide 6
Monovalent Dopants in Bulk Cr2O3

## Slide 7
System | PBE+U (eV) | HSE (eV)
Li-Cr2O3 | +0.71 | -2.78
Na-Cr2O3 | +0.68 | -2.49
K-Cr2O3 | -0.04 | -4.51
Rb-Cr2O3 | +0.13 | -3.82
System | E[active Ov] (eV)
Cr2O3 | 4.11
Li-Cr2O3 | 2.71
Na-Cr2O3 | 2.27
K-Cr2O3 | 2.14
Rb-Cr2O3 | 1.09
Monovalent Dopants in Bulk Cr2O3
Charge Compensation

## Slide 8
Oxygen Migration in Bulk Cr2O3
[010]
[100]
Initial State
Transition State
Final State
[110]

## Slide 9
[010]
Initial State
Transition States
Final State
Initial State
Transition States
Final State
Na
Li
K
Rb
Oxygen Migration in Doped Bulk Cr2O3

## Slide 10
[100]
Initial State
Transition States
Final State
Initial State
Transition States
Final State
Na
Li
K
Rb
Oxygen Migration in Doped Bulk Cr2O3

## Slide 11
[110]
Initial State
Transition States
Final State
Initial State
Transition States
Final State
Na
Li
K
Rb
Oxygen Migration in Doped Bulk Cr2O3

## Slide 12
 | Eact [010] direction (eV) | Eact [100] direction (eV) | Eact [110] direction (eV)
Cr2O3 | +3.30 | +3.30 | +3.30
Li-Cr2O3 | +1.59 | +3.14 | +3.99
Na-Cr2O3 | +2.83 | +2.77 | +4.41
K-Cr2O3 | +3.04 | +3.64 | +3.06
Rb-Cr2O3 | +4.52 | +3.30 | +4.34
Monovalent Doped Bulk Cr2O3

## Slide 13
Divalent Doped Bulk Cr2O3

## Slide 14
 | E[Ovac] (eV)
Undoped Cr2O3 | 4.11
Mg-Cr2O3 | 2.53
Ni-Cr2O3 | 2.45
Cu-Cr2O3 | 1.87
Zn-Cr2O3 | 2.86
2 electrons released: 1 fills oxygen hole, one partially reduces 2 Cr sites
This may result in too favourable oxygen vacancy formation
Divalent Doped Bulk Cr2O3

## Slide 15
2 Mg + O vacancy to compensate holes
E = +1.43 eV (PBE+U)
E = -2.07 eV (HSE06)
Reducing oxygen vacancy
E = +2.38 eV
Divalent Doped Bulk Cr2O3

## Slide 16
2 Cu + O vacancy to compensate holes
E = +0.84 eV (PBE+U)
E = -2.31 eV (HSE06)
Reducing oxygen vacancy
E = +2.86 eV
Divalent Doped Bulk Cr2O3

## Slide 17
 | M-Cr2O3 E[Ovac] (eV) | 2M-Cr2O3 E[active] (eV)
Undoped Cr2O3 | 4.11 | 4.11
Mg doped | 2.53 | 2.38
Ni doped | 2.45 | 2.53
Cu doped | 1.87 | 2.86
Zn doped | 2.88 | 3.21
Clearly more favourable to for Ov to fill oxygen holes
Charge balanced composition promotes formation of reducing Ov compared to undoped Cr2O3
For Ni the energies are the same – no oxygen holes in both compositions
Possible concentration effect on Ni oxidation state?
Mg/Zn – O vacancy reduces two Cr cations to Cr3+
Ni/Cu – Reduction of Cr and dopant
Divalent Doped Bulk Cr2O3 – Reducing Oxygen Vacancy

## Slide 18
High valance dopants can introduce excess electrons:
Which compensation processes will charge balance?
formation of negatively charged defects such as Cr vacancies ()
oxygen interstitials (
Both defects produce hole states that are filled by electrons from the dopant
Higher Valent Doping of Bulk Cr2O3

## Slide 19
High valance dopants
Ti3+, Ti4+
Ce3+, Ce4+
V3+, V 4+, V5+
Zr4+ - non-reducible
One HV dopant: Ti3+, Ce3+, V3+
Bader charge: 9.9 e-, 9.9e-, 11 e-
One Zr dopant: Zr4+, Cr2+
Bader charges:
9.4 e-, 4.6 e-
Higher Valent Doping of Bulk Cr2O3
 | Ef [Cr vac] (eV)
Cr2O3 | 4.59
Ce – Cr2O3 | 2.60
Ti – Cr2O3 | 2.56
V – Cr2O3 | 3.65
Zr – Cr2O3 | 1.70
Ti/Ce/V: 2 O holes + dopant oxidation to +4
Zr: 2 O holes + Cr2+  Cr3+
 | Ef [O vac] (eV)
Cr2O3 | 4.11
Ce – Cr2O3 | 3.89
Ti – Cr2O3 | 4.09
V – Cr2O3 | 4.45
Zr – Cr2O3 | 3.50
Ti/Ce/V: 2 Cr2+
Zr: 3 Cr2+

## Slide 20
Higher Valent Doping of Bulk Cr2O3
Compensate HVD with
 | Ef [3Cr vac] (eV)
3Ce – Cr2O3 | -0.18
3Ti – Cr2O3 | -0.64
3V – Cr2O3 | +0.81 (-1.35 eV HSE)
3Zr – Cr2O3 | -2.02

## Slide 21
 | Ef [O vac] (eV)
Cr2O3 | 4.11
Ce – Cr2O3 | 2.83
Ti – Cr2O3 | 3.04
V – Cr2O3 | 3.83
Zr – Cr2O3 | 3.14
Large ionic radius and favourable Ce3+ formation in Ce-Cr2O3
Higher Valent Doping of Bulk Cr2O3

## Slide 22
Higher Valent Doping of Bulk Cr2O3
Undoped Bulk Chromia has high cost for reducible oxygen vacancy (although similar to CeO2).
Monovalent dopants charge compensated and can tune the migration of O vacancies
Anisotropic O migration – may retard Cr oxidation in stainless steel
Divalent dopants charge compensated
Can enhance formation of reducing oxygen vacancies
Higher valent dopants – depends on their reducibility: M3+ or M4+
Compensated by Cr vacancies
Ce doping can promote reducibility