## Slide 1: Activating carbon dioxide on metal oxide (CrOx, CuOx, CeOx) nanocluster modified TiO2
Michael Nolan, Stephen Rhatigan
Tyndall National Institute, University College Cork, Cork, Ireland
michael.nolan@tyndall.ie
SusChem Project (Ulster, Northwestern): Science Foundation Ireland/DEL/NSF US-Ireland R&D Partnership

## Slide 2
Introduction
Human society is dependent on burning cheap fossil fuels – release CO2
Are there technologies to re-use this otherwise wasted CO2 to produce high value chemicals/fuels?

## Slide 3
  SusChem Project (Ulster, Northwestern): Science Foundation Ireland/DEL/NSF US-Ireland R&D Partnership
  CO2 conversion using combined photo/thermochemical process on modified oxides
  BIOGO project (EU Framework 7 NMP-2013-Large)
  CO2 conversion on metal-modified metal oxides
Introduction

## Slide 4
Introduction
Solar-thermal
  Use a high temperature cycle to reduce a metal oxide
  Concentrated solar energy
  Low(er) temperature chemistry to convert CO2 over reduced metal oxide into chemicals
Front. Energy Res., 02 October 2015 |

## Slide 5
Introduction
CO2 interaction at Cu2O Surfaces (de Leeuw JCP 2016)
CO2@Cu2O(111):O
-0.51 eV
CO2@Cu2O(111):Cu
-1.17 eV -0.97 eV
CO2@Cu2O(110):Cu
-1.17 eV
Low energy surface
High energy surfaces
Bi-pyrochlore (Walker et al. Chem Mat 2016)
Bi-rich surface layer

## Slide 6
Ce5O10
Ce6O12
Eads = -4.75 eV
Eads = -2.47 eV
Clean Rutile (110)
CeO2-modified Rutile TiO2
CO2 interaction at Surface Modified TiO2: CeO2-modified Rutile (110)

## Slide 7
Oxygen Vacancy Formation in CeO2-modified Rutile TiO2
Stoichiometric and reduced CeO2 NCs on (110) surface of rutile TiO2

## Slide 8
Reduced CeO2-x-Modified TiO2
Reduced NCs: charge localisation and DOS plots

## Slide 9
(Ce16O32)-modified TiO2
Evac = -1.59 eV – non-stoichiometric ground state
Evac = +1.23 eV
Moderate cost for reduction
Reduced Ce3+present
Larger CeO2-x-Modified Rutile TiO2

## Slide 10
CuOx-nanocluster modified Anatase (101)
CuO-anatase(101) TiO2
First O vacancy:
Energy cost of -0.13 eV
Second O vacancy:
Energy cost of +0.06 eV
Highly defective CuO:
Mix of Cu+ and Cu2+ species
Third O vacancy
E = + 1.2 eV Reducing
Formation of active defect where CO2 could interact
Mix of Cu+ and Cu2+ species

## Slide 11
CuO-anatase(101) TiO2
CuO-anatase(101) TiO2
2 O vacancies
CuO-anatase(101) TiO2
3 O vacancies

## Slide 12
CuO electronic states in the anatase(101) TiO2 Energy gap
CuOx-nanocluster modified Anatase (101)

## Slide 13
Eads = -2.22 eV
Edesorb = 0.42 eV
(a)
(b)
(c)
(d)
Reduction by interaction with H2
Oxygen vacancy produced by water formation and desorption
Similar to extended CuO (111)
MN PCCP 2014
Eads = -2.78 eV
Edesorb = 0.42 eV
CuOx-nanocluster modified Anatase (101)

## Slide 14
Cr4O6-rutile (110)
Cr4O6-anatase (101)
Cr2O3-nanocluster modified Rutile and Anatase
Cr4+
Ti3+

## Slide 15
Cr4O6-rutile (110)
Cr4O6-anatase (101)
Cr2O3-nanocluster modified Rutile and Anatase

## Slide 16
(a)
(c)
(b)
(d)
(e)
Cr2O3-nanocluster modified Hydroxylated Rutile and Anatase
Cr2+
Cr4+

## Slide 17
Cr2+
Cr4+
Cr4O6-OH-rutile (110)
Cr4O6-OH-anatase (101)

## Slide 18
CO2 Interactions at metal oxide nanocluster modifier Rutile and Anatase TiO2

## Slide 19
CO2 adsorption and activation at CeOx-Rutile
  Adsorption energies Up to -0.9 eV (Ce5O8)
  Up to -1.7 eV (Ce6O10)
  C-O bonds elongated by up to 10%
  O-C-O bending
CO2 adsorption at oxygen vacancy sites

## Slide 20
CO2 adsorption and activation at CeOx-Rutile
CO2 adsorption at oxygen vacancy sites:
  Adsorption energy -2.65 eV
  C-O bonds elongated by 0.10 → 0.12 Å (10%)
  O-C-O bending
(Ce16O32)-modified TiO2

## Slide 21
CO2@Cu10O8-anatase
III E = -2.42 eV
CO2 adsorption and activation at CuOx-Rutile
Cu10O8-anatase
CO2@Cu10O8-anatase + H2
II E = -0.70 eV

## Slide 22
Cu10O8-anatase
Cu10O7-anatase

## Slide 23
CO2 adsorption and activation at CuOx-Rutile
Cu10O7-anatase
CO2@Cu10O7-anatase
on TiO2 E = -1.75 eV
CO2@Cu10O7-anatase II
E = -1.00 eV
Cu10O7-Anatase (101) | 
Cu10O7-Anatase (101) + CO2 CO2 vibrational modes / cm-1 | 1622, 1266, 623, 603
Free CO2 vibrational modes / cm-1 | 2354, 1325, 632 (degenerate)

## Slide 24
Cr4O6-Rutile (110) CO2 I
Eads = -0.63 eV
Cr4O6-Rutile (110) CO2 II
Eads = -0.91 eV
Cr4O6-H2O-Rutile (110) CO2 I
Eads = -0.92 eV
Cr4O6-H2O-Rutile (110) CO2 II
Eads = -0.31 eV
CO2 adsorption and activation at Cr2O3 -Rutile
Cr4O6- Rutile (110) | 
Cr4O6-Rutile (110) + CO2 CO2 vibrational modes / cm-1 | 1589, 1226, 921, 803
Cr4O6-H2O-Rutile (110) + CO2 CO2 vibrational modes / cm-1 | 1774, 1152, 899, 796
Free CO2 vibrational modes / cm-1 | 2354, 1325, 632 (degenerate)

## Slide 25
Cr4O6-rutile (110)
Cr4O6-OH-rutile (110)
Cr4O6-antase (101)
Cr4O6-OH-anatase (101)

## Slide 26
Cr4O6-Anatase (101) CO2 I
Eads = -2 eV
Cr4O6-Anatase (101) CO2 II
Eads = -0.1 eV
CO formed directly
Cr4O6-H2O-Anatase (101) CO2 I
Eads = -0.71 eV
Cr4O6-H2O-Anatase (101) CO2 II
Eads = -1.11 eV
CO2 adsorption and activation at Cr2O3 -Anatase
Cr4O6- Anatase (101) | 
Bi4O6-Anatase (101) + CO2 CO2 vibrational modes / cm-1 | 1617, 1210, 915, 906
Cr4O6-H2O-Anatase (101) + CO2 CO2 vibrational modes / cm-1 | 1642, 1243, 959, 777
Free CO2 vibrational modes / cm-1 | 2354, 1325, 632 (degenerate)

## Slide 27
Summary
DFT studies of oxide nanocluster modified rutile/anatase TiO2 for CO2 activation
Supported CeO2 is off-stoichiometric with Ce3+
Supported CuO is off-stoichiometric with mixed Cu+/Cu2+
All supported oxide clusters adsorb and activate CO2
Bending of O-C-O angle to ~127-130o; elongation of C-O distances
Strong red shift in C=O stretch of up to 750cm-1 and lift O-C-O bend degeneracy

## Slide 28
COOH + OH
COOH + OH
E = -1.73 eV
Form H2O
CO2 adsorption and activation at CuOx-Rutile
CO2@Cu10O7-anatase II + H2 III
E (H2) = - 3.85 eV

## Slide 29
CO2@Cu10O7-anatase II + H2 on TiO2 II
E (H2) = - 4.46eV
COOH + OH
E = 0 eV
Iso-energetic
COOH + OH
Form H2O
Relax to COOH + OH
CO2 adsorption and activation at CuOx-Rutile