De Jong et al.

TOXICITY OF COPPER OXIDE AND BASIC COPPER CARBONATE NANOPARTICLES AFTER SHORT TERM ORAL EXPOSURE IN RATS

Supplementary Figures and Tables.

Comparison CuO-NP dispersion freshly prepared versus 24 hours after preparation (102.4 mg/mL).

Comparison Cu2CO3(OH)2-NP dispersion freshly prepared versus 72 hours after preparation (25.6 mg/mL).

Supplementary Figure 1. Size distribution of CuO NP (top image ) and Cu2CO3(OH)2 NP (bottom image) dispersions freshly prepared and after storage for 24 hours and 72 hours, respectively, as measured by CPS Disc Centrifuge™. Data are presented in number metrics.

A

B

Supplementary Figure 2. Morphology of pristine and transformed NPs by transmission electron microscopy (TEM). The top row depicts  Cu2CO3(OH)2 NPs (a,b,c), while the bottom row is CuO NPs (d, e, f). The particles are illustrated  before (a,b) and after dissolution testing at 37°C in either pH1.6 stomach simulant (b,e) or pH5.8 FeSSIF-V2 middle intestine simulant (c,f.). EDXS was unable to detect Cu content in the samples b and e.

Supplementary Figure 3 Effects on bone marrow. The left image represents the bone marrow of a control animal. The right image indicates myeloid cell proliferation of the bone marrow at day 6 of an animal treated with Cu2CO3(OH)2 NPs 128 mg/kg b.w. for 5 consecutive days (days 1-5). Note abundance of myeloid cell lineage (*) compared to erythroid cell lineage (#).

Supplementary Table 1. Study design of five day oral toxicity study in rats.

| Study day | Days 1 to 5 | Day 6 | Day 7-25 | Day 26 |
| --- | --- | --- | --- | --- |
| CuO NPs | Exposure by oral gavage (dose mg/kg) | Autopsy | Recovery | Autopsy |
|  | 0 | N=4 |  | N=4 |
|  | 1 | N=4 |  | N=4 |
|  | 2 | N=4 |  | N=4 |
|  | 4 | N=4 |  | N=4 |
|  | 8 | N=4 |  | N=4 |
|  | 16 | N=4 |  | N=4 |
|  | 32 | N=4 |  | N=4 |
| Pilot study | 64 | N=2 |  |  |
| Extra study | 512 | N=4 |  |  |
| Cu2CO3(OH)2 NPs | Exposure by oral gavage (dose mg/kg) | Autopsy | Recovery | Autopsy |
| Dose (mg/kg) | 0 | N=4 |  | N=4 |
|  | 4 | N=4 |  | N=4 |
|  | 8 | N=4 |  | N=4 |
|  | 16 | N=4 |  | N=4 |
|  | 32 | N=4 |  | N=4 |
|  | 64 | N=4 |  | N=4 |
|  | 128 | N=4+4a |  |  |

- N=4 unscheduled autopsy in due to overt signs of toxicity

Supplementary Table 2A Body and organ weight of male rats at day 6 after 5 consecutive days of oral administration of CuO NPs.

| CuO NPs |  |  |  |  |  |  |  |  | Pilot Study |  | Extra Study |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose | 0 mg/kg | 1 mg/kg | 2 mg/kg | 4 mg/kg | 8 mg/kg | 16 mg/kg | 32 mg/kg |  | 64 mg/kg |  | 512 mg/kga |
| Body weight (g) | 275 ± 8 | 275 ± 25 | 292 ±9 | 310 ± 46 | 288 ±8 | 290 ± 7 | 280 ± 23 |  | 288 ± 4 |  | 334 ± 43 |
| Lung | 1.30 ± 0.12 | 1.33 ± 0.10 | 1.37 ± 0.09 | 1.53 ± 0.09 (3) | 1.53 ± 0.08 | 1.39 ± 0.08 | 1.35 ± 0.10 |  | 1.29 (1) |  | 1.48 ± 0.09 |
| Heart | 0.881 ± 0.02 | 0.938 ± 0.06 | 0.957 ± 0.02 | 0.934 ± 0.06 | 0.945 ± 0.02 | 0.976 ± 0.03 | 0.931 ± 0.06 |  | 0.934 ± 0.08 |  | 1.097 ± 0.16 |
| Liver | 10.67 ± 0.52 | 11.00 ± 0.47 (3) | 11.19 ± 0.62 | 11.01 ± 0.63 | 11.22 ± 0.39 | 10.52 ±0.80 | 10.89 ± 1.14 |  | 11.01 ± 0.19 |  | 12.06 ± 2.21 |
| Kidney (L+R) | 2.18 ± 0.08 | 2.28 ± 0.14 (3) | 2.31 ± 0.10 | 2.22 ± 0.18 | 2.33 ± 0.06 | 2.33 ± 0.09 | 2.14 ± 0.26 |  | 2.18 ± 0.08 |  | 2.25 ± 0.25 |
| Spleen | 0.50 ± 0.04 | 0.50 ± 0.04 | 0.53 ± 0.03 | 0.52 ± 0.04 | 0.53 ±0.03 | 0.54 ± 0.03 | 0.54 ± 0.04 |  | 0.51 ± 0.06 |  | 0.855 ± 0.22 |
| Thymus | 0.503 ± 0.04 | 0.537 ± 0.09 | 0.552 ± 0.04 | 0.591 ± 0.02 | 0.544 ± 0.04 (3) | 0.530 ±0.07 | 0.527 ± 0.06 |  | 0.478 ± 0.03 |  | 0.526 ± 0.21 |
| Mesenteric Lymph Node | 0.126 ± 0.01 | 0.157 ± 0.05 | 0.161 ± 0.03 | 0.154 ± 0.02 | 0.144 ± 0.02 | 0.164 ± 0.03 | 0.155 ± 0.02 |  | 0.125 ± 0.02 |  | 0.263 ± 0.07 |
| Testes (L+R) | 2.66 ± 0.18 | 2.50 ±0.64 | 2.83 ± 0.11 | 2.93 ± 0.10 | 2.71 ± 0.22 | 2.80 ± 0.11 | 2.78 ± 0.14 |  | 2.79 ± 0.06 |  | 3.31 ± 0.30 |
| Brain | 2.00 ± 0.03 | 2.03 ± 0.01 | 20.6 ± 0.02 | 2.02 ± 0.03 | 2.04 ±0.04 | 2.07 ± 0.04(3) | 20.3 ± 0.06 |  | 2.06 (1) |  | 2.11 ± 0.03 |
| Adrenals | 0.032 ± 0.001 | 0.034 ± 0.005 | 0.037 ± 0.003 | 0.037 ± 0.002 | 0.039 ± 0.004 (2) | 0.037 ± 0.003 | 0.039 ± 0.003 |  | - |  | 0.058 ± 0.005 |

Values represent mean ± SD (weight in g). The number of animals per group is 4 (n=4) unless otherwise indicated in the table within brackets. For the dose of 64 mg/kg in the pilot study two (n=2) animals were evaluated. Autopsy was conducted at day 6 (24 hours after the last oral administration).

a) Animals with dose 512 mg/kg as extra group were treated without concurrent contemporary control.

Supplementary Table 2B Body and organ weights of male rats at day 26 after 5 consecutive days of oral administration of CuO NPs.

| CuO NPs |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Dose | 0 mg/kg | 1 mg/kg | 2 mg/kg | 4 mg/kg | 8 mg/kg | 16 mg/kg | 32 mg/kg |
| Body weight (g) | 343 ± 7 | 332 ± 9 | 351 ±14 | 318 ± 56 | 345 ± 12 | 329 ± 41 | 341 ± 14 |
| Lung | 1.47 ± 0.08 | 1.54 ± 0.20 | 1.51 ± 0.07 | 1.50 ± 0.16 (3) | 1.53 ± 0.10 | 1.41 ± 0.18 | 1.52 ± 0.17 |
| Heart | 1.011 ± 0.04 | 0.987 ± 0.08 | 1.037 ± 0.08 | 0.992 ± 0.07 | 1.012 ± 0.08 | 1.052 ± 0.04 | 1.019 ± 0.06 |
| Liver | 12.36 ± 0.27 | 11.67 ±0.72 | 12.40 ± 0.70 | 11.03 ± 1.99 | 12.80 ± 1.12 | 11.18 ± 2.24 | 11.92 ± 0.42 |
| Kidney (L+R) | 2.61 ±0.06 | 2.46 ± 0.25 | 2.61 ± 0.12 | 2.38 ± 0.42 | 2.38 ± 0.32 | 2.45 ± 0.52 | 2.78 ± 0.39 |
| Spleen | 0.582 ± 0.03 | 0.521 ±0.04 | 0.582 ± 0.03 | 0.436 ± 0.17 | 0.595 ± 0.03 | 0.540 ± 0.05 | 0.599 ± 0.11 |
| Thymus | 0.483 ± 0.07 | 0.407 ± 0.04 | 0.486 ± 0.04 | 0.466 ± 0.06 | 0.485 ± 0.03 | 0.433 ± 0.13 | 0.493 ± 0.06 |
| Mesenteric Lymph Node | 0.189 ± 0.04 | 0.173 ± 0.01 | 0.200 ± 0.01 | 0.169 ± 0.01 | 0.161 ± 0.02 | 0.159 ± 0.02 | 0.204 ± 0.001 |
| Testes (L+R) | 2.97 ± 0.09 | 2.86 ± 0.06 | 3.10 ± 0.21 | 2.77 ± 0.41 | 2.89 ± 0.24 | 2.91 ± 0.37 | 2.98 ±0.07 |
| Brain | 2.14 ± 0.02 | 2.09 ± 0.04 | 2.15 ± 0.02 | 2.08 ± 0.09 | 2.10 ± 0.03 | 2.08 ± 0.11 | 2.18 ± 0.07 |
| Adrenals | 0.041 ± 0.004 | 0.037 ± 0.003 | 0.042 ± 0.002 | 0.042 ± 0.002 | 0.040 ± 0.007 | 0.040 ± 0.005 | 0.040 ± 0.003 |

Values represent mean ± SD (weight in g). The number of animals per group is 4 (n=4) unless otherwise indicated in the table within brackets. Autopsy was conducted at day 26 (21 days after the last oral administration).

Supplementary Table 2C Body and organ weight in male rats at days 6/7 after 5 consecutive days of oral administration of Cu2CO3(OH)2 NPs.

| Cu2CO3(OH)2 NPs |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose | 0 mg/kg | 4 mg/kg | 8 mg/kg | 16 mg/kg | 32 mg/kg | 64 mg/kg | 128 mg/kg |  | 128 mg/kga |  |  |
| Body weight (g) | 345 ± 11 | 385 ±24 | 394 ± 58 | 367 ± 15 | 362 ±11 | 344 ± 29 | 327 ± 73 |  | 290 ± 16** |  |  |
| Lung | 1.48 ± 0.11 | 1.56 ± 0.15 | 1.50 ± 0.04 | 1.50 ± 0.08 | 1.36 ± 0.35 | 1.51 ± 0.53 | 1.46 ± 0.17 |  | 1.34 ± 0.16 |  |  |
| Heart | 1.210 ± 0.05 | 1.279 ± 0.07 | 1.300 ± 0.08 | 1.244 ±0.09 | 1.140 ± 0.06 | 1.185 ± 0.16 | 1.002 ± 0.14* |  | 0.928 ± 0.02** |  |  |
| Liver | 13.40 ± 0.57 | 15.68 ± 1.52 | 15.14 ± 1.24 | 14.79 ± 0.25 | 14.42 ± 0.90 | 14.15 ± 2.22 | 10.79 ± 1.22** |  | 10.43 ± 1.33** |  |  |
| Kidney (L+R) | 2.23 ± 0.15 | 2.35 ± 0.14 | 2.38 ± 0.05 | 2.26 ± 0.11 | 2.21 ± 0.25 | 2.29 ± 0.30 | 2.00 ± 0.75 |  | 2.14 ± 0.45 |  |  |
| Spleen | 0.992 ± 0.09 | 1.040 ± 0.16 | 1.032 ± 0.20 | 0.955 ± 0.09 | 1.020 ± 0.26 | 1.059 ± 0.15 | 0.508 ± 0.08** |  | 0.540 ± 0.16** |  |  |
| Thymus | 0.706 ± 0.13 | 0.789 ± 0.10 | 0.826 ± 0.04 | 0.745 ± 0.16 | 0.798 ± 0.21 | 0.717 ± 0.19 | 0.221 ± 0.06** |  | 0.192 ± 0.06** |  |  |
| Mesenteric Lymph Node | 0.254 ± 0.06 | 0.265 ± 0.05 | 0.227 ± 0.03 | 0.188 ± 0.03 | 0.263 ± 0.03 | 0.224 ± 0.08 | 0.210 ± 0.04 |  | 0.222 ± 0.06 |  |  |
| Testes (L+R) | 3.33 ± 0.23 | 3.42 ± 0.37 | 3.26 ± 0.38 | 2.66 ± 0.17 | 3.11 ± 0.28 | 3.29 ± 0.37 | 3.02 ± 0.29 |  | 3.06 ± 0.34 |  |  |
| Brain | 1.92 ± 0.03 | 1.94 ± 0.05 | 1.88 ± 0.02 | 1.93 ± 0.08 | 1.88 ± 0.11 | 1.91 ± 0.08 | 1.86 ± 0.07 |  | 1.84 ± 0.11 |  |  |
| Adrenals | 0.043 ± 0.004 | 0.051 ± 0.009 | 0.051 ± 0.006 | 0.051 ± 0.006 | 0.052 ± 0.005 | 0.051 ± 0.004 | 0.071 ± 0.015* |  | 0.063 ± 0.008** |  |  |

Values represent mean ± SD (weight in g). The number of animals per group is 4 (n=4) unless otherwise indicated in the table within brackets. Significant differences compared to vehicle treated animals. *p<0.05, **P<0.01 (ANOVA). Autopsy was conducted at day 6/ 7 (128 mg/kg b.w.)  (24 or 48 hours after the last oral administration).

a)Unscheduled autopsy of dose group of 128 mg/kg at days 6/7 after treatment in view of poor condition of the animals.

Supplementary Table 2D Body and organ weight in male rats at day 26 after 5 consecutive days of oral administration of Cu2CO3(OH)2 NPs - At day 26 (21 days after the last administration).

| Cu2CO3(OH)2 NPs |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Dose | 0 mg/kg | 4 mg/kg | 8 mg/kg | 16 mg/kg | 32 mg/kg | 64 mg/kg |
| Body weight (g) | 457 ± 13 | 456 ± 24 | 426 ± 28 | 465 ± 50 | 448 ± 37 | 455 ± 26 |
| Lung | 1.81 ± 0.18 | 1.74 ± 0.03 | 1.44 ± 0.33 | 1.77 ± 0.20 | 1.60 ± 0.09 | 1.46 ± 0.24 |
| Heart | 1.356 ± 0.06 | 1.429 ± 0.08 | 1.342 ± 0.05 | 1.443 ± 0.16 | 1.402 ± 0.04 | 1.414 ± 0.11 |
| Liver | 16.27 ± 1.71 | 15.82 ± 0.85 | 14.73 ± 1.10 | 17.72 ± 3.15 | 15.82 ± 2.39 | 16.56 ± 1.94 |
| Kidney (L+R) | 2.70 ± 0.19 | 2.68 ± 0.26 | 2.58 ± 0.39 | 2.59 ± 0.15 | 2.62 ± 0.24 | 2.56 ± 0.30 |
| Spleen | 1.111 ± 0.17 | 1.132 ± 0.20 | 1.066 ± 0.10 | 1.145 ± 0.22 | 1.063 ± 0.11 | 1.034 ± 0.12 |
| Thymus | 0.777 ± 0.20 | 0.575 ± 0.07 | 0.629 ± 0.05 | 0.721 ± 0.15 | 0.720 ± 0.15 | 0.695 ± 0.12 |
| Mesenteric Lymph Node | 0.208 ± 0.02 | 0.210 ± 0.04 | 0.194 ± 0.02 | 0.227 ± 0.05 | 0.216 ± 0.05 (3) | 0.226 ± 0.03 |
| Testes (L+R) | 3.50 ± 0.17 | 3.12 ± 0.35 | 3.53 ± 0.06 | 3.64 ± 0.21 | 3.40 ± 0.13 | 3.42 ± 0.26 |
| Brain | 1.99 ± 0.08 | 2.00 ± 0.05 | 1.97 ± 0.04 | 2.03 ± 0.02 | 1.97 ± 0.07 | 1.99 ± 0.09 |
| Adrenals | 0.053 ± 0.005 (3) | 0.053 ± 0.005 | 0.051 ± 0.010 | 0.046 ± 0.010 | 0.050 ± 0.006 | 0.052 ± 0.004 |

Values represent mean ± SD (weight in g). The number of animals per group is 4 (n=4) unless otherwise indicated in the table within brackets. Autopsy was conducted at day 26 (21 days after the last oral administration).

Supplementary Table 3A Haematology in male rats at day 6 after 5 consecutive days of oral administration of CuO NPs.

| CuO NPs |  |  |  |  |  |  |  |  | Pilot Study |  | Extra Study |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose | 0 mg/kg | 1 mg/kg | 2 mg/kg | 4 mg/kg | 8 mg/kg | 16 mg/kg | 32 mg/kg |  | 64 mg/kg |  | 512 mg/kga |
| WBC x109/L | 5.07 ± 0.53 | 4.46 ± 0.52 | 5.27 ± 0.7 | 3.92 ± 0.40*b | 4.40 ± 0.41 | 4.39 ± 0.51 | 3.98 ± 0.24* |  | 2.89 ± 0.41** |  | 9.53 ± 1.47 |
| RBC x1012/L | 8.03 ± 0.29 | 7.96 ± 0.15 | 8.00 ± 0.12 | 8.12 ± 0.10 | 7.84 ± 0.27 | 7.81 ± 0.12 | 7.68 ± 0.21 |  | 7.50 ± 0.12* |  | 8.33 ± 0.92 |
| HgB Mmol/L | 8.60 ± 0.36 | 8.38 ± 0.40 | 8.60 ± 0.16 | 8.65 ± 0.13 | 8.43 ± 0.26 | 8.33 ± 0.15 | 8.05 ± 0.21 |  | 8.07 ± 0.19* |  | 9.25 ± 0.85 |
| Hct L/L | 0.415 ± 0.02 | 0.403 ± 0.02 | 0.410 ± 0.01 | 0.420 ± 0.02 | 0.402 ± 0.02 | 0.403 ± 0.01 | 0.400 ± 0.00 |  | 0.380 ±0.00* |  | 0.218 ± 0.02 |
| MCV fl | 52 ± 0.7 | 50 ± 1.7 | 51 ± 0.5 | 51 ± 0.6 | 52 ± 0.9 | 52 ± 0.4 | 52 ± 1.3 |  | 51 ± 0.1 |  | 52 ± 1.6 |
| MCH fmol | 1.07 ± 0.01 | 1.05 ± 0.03 | 1.08 ± 0.02 | 1.07 ± 0.01 | 1.07 ± 0.01 | 1.07 ± 0.01 | 1.05 ± 0.00 |  | 1.07 ± 0.01 |  | 1.12 ± 0.02 |
| MCHC Mmol/L | 20.62 ± 0.22 | 20.79 ± 0.20 | 20.97 ± 0.25 | 20.68 ± 0.24 | 20.76 ± 0.31 | 20.60 ± 0.17 | 20.46 ± 0.48 |  | 20.77 ± 0.17 |  | 21.24 ± 0.33 |
| RDW % | 11.41 ± 0.19 | 11.69 ± 0.59 | 11.59 ± 0.19 | 11.44 ± 0.18 | 11.36 ± 0.19 | 11.44 ± 0.18 | 11.58 ± 0.11 |  | 11.60 ± 0.14 |  | 11.96 ± 0.21 |
| HDW Mmol/L | 1.45 ± 0.06 | 1.50 ± 0.04 | 1.51 ± 0.01 | 1.47 ± 0.02 | 1.43 ± 0.04 | 1.48 ± 0.07 | 1.43 ± 0.10 |  | 1.43 ± 0.05 |  | 1.67 ± 0.08 |
| PLT x109/L | 739 ± 36 | 577 ± 204 | 730 ± 32 | 728 ± 18 | 739 ± 9 | 692 ± 146 | 766 ± 41 |  | 739 ± 45 |  | 1196 ± 236 |
| MPV fl | 6.70 ± 0.23 | 7.56 ± 0.97 | 6.90 ± 0.25 | 6.46 ± 0.29 | 6.90 ± 0.43 | 7.15 ± 0.95 | 6.45 ± 0.42 |  | 6.82 ± 0.26 |  | 7.56 ± 0.70 |
| Neutrophils % | 9.9 ± 0.6 | 13.0 ± 3.0 | 11.1 ± 1.7 | 8.8 ± 1.1 | 11.7 ± 0.8 | 13.0 ± 2.1 | 11.2 ± 1.1 |  | 15.0 ± 2.1 |  | 27.5 ± 13.6 |
| Lymphocytes % | 86.5 ± 0.7 | 80.8 ±4.6 | 84.7 ± 2.4 | 85.5 ± 2.0 | 83.0 ± 1.0 | 81.4 ± 2.8 | 83.0 ± 0.8* |  | 81.4 ± 2.6 |  | 67.2 ± 15.4 |
| Monocytes % | 1.54 ± 0.38 | 1.80 ± 0.54 | 2.01 ± 0.14 | 1.66 ± 0.21 | 1.37 ± 0.13 | 1.71 ± 0.20 | 1.78 ± 0.32 |  | 1.52 ± 0.26 |  | 2.56 ± 1.11 |
| Eosinophils % | 1.61 ± 0.70 | 3.99 ± 1.51 | 1.66 0.69 | 3.65 ± 1.96 | 3.76 ± 0.32 | 3.56 ± 1.62 | 3.68 ± 0.18** |  | 1.80 ± 0.80 |  | 0.64 ± 0.38 |
| LUC % | 0.30 ± 0.12 | 0.33 ± 0.15 | 0.46 ± 0.08 | 0.41 ± 0.11 | 0.23 ± 0.05 | 0.25 ± 0.07 | 0.35 ± 0.28 |  | 0.18 ± 0.02 |  | 2.01 ± 1.38 |
| Basophils % | 0.05 ± 0.04 | 006 ± 0.06 | 0.05 ± 0.10 | 0.03 ± 0.05 | 0.09 ± 0.04 | 0.06 ± 0.05 | 0.05 ± 0.00 |  | 0.10 ± 0.09 |  | 0.08 ± 0.03 |
| Reticulocytes % | 2.70 ± 0.41 | 2.69 ± 0.44 | 2.85 ± 0.11 | 2.49 ± 0.34 | 2.47 ± 0.25 | 2.98 ± 0.38 | 2.57 ± 0.5 |  | 2.07 ± 0.30 |  | 1.66 ± 1.04 |
| Neutrophils x109/L | 0.50 ± 0.08 | 0.58 ± 0.15 | 0.59 ± 0.16 | 0.35 ± 0.07 | 0.51 ± 0.07 | 0.58 ± 0.16 | 0.44 ± 0.01 |  | 0.44 ± 0.13 |  | 2.49 ± 1.09 |
| Lymphocytes x109/L | 4.39 ± 0.44 | 3.62 ± 0.53 | 4.45 ± 0.48 | 3.36 ± 0.38 | 3.64 ± 0.33 | 3.56 ± 0.31 | 3.30 ± 0.23* |  | 2.35 ± 0.26** |  | 6.56 ± 2.54 |
| Monocytes x109/L | 0.08 ± 0.02 | 0.08 ± 0.02 | 0.11 ± 0.02 | 0.07 ± 0.01 | 0.06 ± 0.01 | 0.08 ± 0.02 | 0.07 ± 0.01 |  | 0.04 ± 0.00 |  | 0.23 ± 0.09 |
| Eosinophils x109/L | 0.08 ± 0.04 | 0.17 ± 0.05 | 0.09 ± 0.05 | 0.14 ± 0.07 | 0.16 ± 0.00 | 0.16 ± 0.07 | 0.15 ± 0.02 |  | 0.05 ± 0.03 |  | 0.06 ± 0.03 |
| LUC x109/L | 0.01 ± 0.01 | 0.01 ± 0.01 | 0.02 ± 0.00 | 0.02 ± 0.01 | 0.01 ± 0.00 | 0.01 ± 0.01 | 0.02 ± 0.01 |  | 0.00 ± 0.00 |  | 0.01 ± 0.01 |
| Basophils x109/L | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 |  | 0.00 ± 0.00 |  | 0.18 ± 0.10 |
| Reticulocytes x1012/L | 0.22 ± 0.03 | 0.21 ± 0.03 | 0.23 ± 0.01 | 0.20 ± 0.03 | 0.19 ± 0.01 | 0.23 ± 0.03 | 0.20 ± 0.02 |  | 0.16 ± 0.02 |  | 0.13 ± 0.07 |

Values represent mean ± SD (n=4). The pilot study (dose 64 mg/kg b.w. was performed with n=2. For the dose of 32 mg/kg b.w. n=2 animals could be evaluated. Blood samples were obtained at day 6 (24 hours after the last administration).

- Animals with dose 512 mg/kg as extra group were treated without concurrent contemporary control.

- One sided students t-test, * P<0.05, ** p<0.01, *** p<0.01.

Supplementary Table 3B Haematology in male rats at day 26 after 5 consecutive days of oral administration of CuO NPs.

| CuO NPs |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose | 0 mg/kg |  | 1 mg/kg | 2 mg/kg | 4 mg/kg | 8 mg/kg | 16 mg/kg | 32 mg/kg |
| WBC x109/L | 5.40 ± 0.99 |  | 5.95 ± 1.18 | 5.15 ± 0.31 | 4.87 ± 0.80 | 6.44 ± 0.96 | 5.60 ± 1.13 | 5.33 ± 0.99 |
| RBC x1012/L | 8.54 ± 0.25 |  | 8.55 ± 0.06 | 8.59 ± 0.16 | 8.66 ± 0.27 | 8.69 ± 0.15 | 8.77 ± 0.31 | 8.28 ± 0.96 |
| HgB Mmol/L | 8.73 ± 0.22 |  | 8.57 ± 0.06 | 8.55 ± 0.29 | 8.73 ± 0.31 | 8.85 ± 0.25 | 8.87 ± 0.31 | 8.44 ± 0.83 |
| Hct L/L | 0.410 ± 0.01 |  | 0.413 ± 0.01 | 0.405 ± 0.01 | 0.413 ± 0.01 | 0.425 ± 0.01 | 0.427 ± 0.01 | 0.398 ± 0.04 |
| MCV fl | 49 ± 0.5 |  | 48 ± 0.4 | 47 ± 0.3 | 47 ± 0.6 | 49 ± 0.3 | 48 ± 0.1 | 48 ± 0.8 |
| MCH fmol | 1.02 ± 0.02 |  | 1.01 ± 0.02 | 1.00 ± 0.01 | 1.01 ± 0.01 | 1.02 ± 0.01 | 1.01 ± 0.01 | 1.02 ± 0.02 |
| MCHC Mmol/L | 20.95 ± 0.14 |  | 20.92 ± 0.14 | 21.00 ± 0.28 | 21.26 ± 0.27 | 20.94 ± 0.14 | 21.07 ± 0.07 | 21.21 ± 0.19 |
| RDW % | 11.49 ± 0.15 |  | 11.55 ± 0.09 | 11.59 ± 0.14 | 11.55 ± 0.22 | 11.48 ± 0.12 | 11.57 ± 0.15 | 11.59 ± 0.19 |
| HDW Mmol/L | 1.71 ± 0.03 |  | 1.74 ± 0.01 | 1.73 ± 0.03 | 1.80 ± 0.05 | 1.69 ± 0.03 | 1.75 ± 0.03 | 1.69 ± 0.04 |
| PLT x109/L | 707 ± 20 |  | 714 ± 28 | 693 ± 26 | 706 ± 23 | 678 ± 60 | 681 ± 19 | 749 ± 69 |
| MPV fl | 7.14 ± 0.29 |  | 6.98 ± 0.24 | 6.93 ± 0.19 | 7.15 ± 0.44 | 7.11 ± 0.28 | 7.23 ± 0.51 | 6.83 ± 0.17 |
| Neutrophils % | 11.4 ± 1.3 |  | 12.0 ± 0.2 | 10.8 ± 2.0 | 10.1 ± 1.3 | 12.0 ± 2.1 | 11.6 ± 2.9 | 10.8 ± 2.4 |
| Lymphocytes % | 84.1 ± 1.8 |  | 84.0 ± 1.1 | 85.0 ± 2.6 | 86.6 ± 2.5 | 84.0 ± 2.4 | 85.0 ± 3.5 | 83.5 ± 4.2 |
| Monocytes % | 1.41 ± 0.06 |  | 2.00 ± 0.43 | 1.88 ± 0.48 | 1.60 ± 0.40 | 1.78 ± 0.46 | 1.47 ± 0.38 | 1.85 ± 0.48 |
| Eosinophils % | 2.68 ± 2.08 |  | 1.43 ± 0.68 | 1.66 ± 0.21 | 1.35 ± 0.74 | 1.75 ± 0.26 | 1.33 ± 0.25 | 3.25 ± 2.51 |
| LUC % | 0.39 ± 0.22 |  | 0.45 ± 0.13 | 0.58 ± 0.21 | 0.38 ± 0.16 | 0.45 ± 0.19 | 0.55 ± 0.26 | 0.42 ± 0.31 |
| Basophils % | 0.06 ± 0.03 |  | 0.07 ± 0.03 | 0.03 ± 0.03 | 0.08 ± 0.03 | 0.04 ± 0.05 | 0.07 ± 0.06 | 0.12 ± 0.04 |
| Reticulocytes % | 2.15 ± 0.16 |  | 2.22 ± 0.18 | 2.12 ± 0.06 | 2.17 ± 0.27 | 2.00 ± 0.12 | 2.05 ± 0.20 | 2.24 ± 0.43 |
| Neutrophils x109/L | 0.62 ± 0.17 |  | 0.72 ± 0.14 | 0.56 ± 0.12 | 0.48 ± 0.07 | 0.76 ± 0.04 | 0.67 ± 0.30 | 0.59 ± 0.24 |
| Lymphocytes x109/L | 4.54 ± 0.86 |  | 5.01 ± 1.06 | 4.38 ± 0.21 | 4.22 ± 0.75 | 5.43 ± 0.97 | 4.73 ± 0.76 | 4.43 ± 0.62 |
| Monocytes x109/L | 0.08 ± 0.01 |  | 0.12 ± 0.01 | 0.10 ± 0.03 | 0.08 ± 0.02 | 0.11 ± 0.01 | 0.08 ± 0.03 | 0.09 ± 0.00 |
| Eosinophils x109/L | 0.14 ± 0.08 |  | 0.08 ± 0.02 | 0.08 ± 0.02 | 0.07 ± 0.03 | 0.12 ± 0.03 | 0.08 ± 0.03 | 0.19 ± 0.17 |
| LUC x109/L | 0.02 ± 0.02 |  | 0.03 ± 0.01 | 0.03 ± 0.02 | 0.02 ± 0.01 | 0.03 ± 0.01 | 0.03 ± 0.02 | 0.02 ± 0.01 |
| Basophils x109/L | 0.00 ± 0.00 |  | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 |
| Reticulocytes x1012/L | 0.18 ± 0.01 |  | 0.19 ± 0.01 | 0.18 ± 0.00 | 0.19 ± 0.02 | 0.17 ± 0.01 | 0.18 ± 0.02 | 0.18 ± 0.01 |

Values represent mean ± SD (n=4). Blood samples were obtained at day 26 (21 days after the last administration).For some animals blood was not available for evaluation. The number of animals is n=3 for the dose groups  of  1, 4 and 16 mg/kg b.w.

Supplementary Table 3C. Haematology in male rats at day 6 after 5 consecutive days of oral administration of Cu2CO3(OH)2 NPs.

| Cu2CO3(OH)2 NPs |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose | 0 mg/kg | 4 mg/kg | 8 mg/kg | 16 mg/kg | 32 mg/kg | 64 mg/kg | 128 mg/kg |  | 128 mg/kga |
| WBC x109/L | 8.29 ± 1.56 (3) | 13.10 ± 1.75 | 11.46 ± 0.55 | 10.78 ± 1.72 | 13.48 ± 3.13 | 16.37 ± 4.85* | 17.49 ± 7.8* |  | 18.35 ± 6.8* |
| RBC x1012/L | 7.32 ± 0.26 | 7.57 ± 0.3 | 7.27 ± 0.4 | 7.20 ± 0.35 | 7.32 ± 0.36 | 7.51 ± 0.25 | 9.36 ± 1.5** |  | 8.38 ± 0.17 |
| HgB Mmol/L | 8.23 ± 0.4 | 8.48 ± 0.56 | 8.45 ± 0.31 | 8.30 ± 0.35 | 8.20 ± 0.39 | 8.68 ± 0.22 | 10.0 ± 0.92** |  | 9.43 ± 0.21* |
| Hct L/L | 0.40 ± 0.02 | 0.41 ± 0.03 | 0.41 ± 0.01 | 0.40 ± 0.02 | 0.40 ± 0.02 | 0.42 ± 0.01 | 0.48 ± 0.05** |  | 0.45 ± 0.01* |
| MCV fl | 54 ± 1 | 54 ± 1 | 57 ± 3 | 55 ± 1 | 54 ± 1 | 55 ± 1 | 52 ± 4 |  | 54 ± 2 |
| MCH fmol | 1.12 ± 0.02 | 1.12 ± 0.04 | 1.17 ± 0.06 | 1.15 ± 0.03 | 1.12 ± 0.01 | 1.16 ± 0.04 | 1.08 ± 0.11 |  | 1.12 ± 0.05 |
| MCHC Mmol/L | 20.6 ± 0.11 | 20.7 ± 0.23 | 20.3 ± 0.36 | 20.8 ± 0.10 | 20.6 ± 0.11 | 20.9 ± 0.46 | 20.8 ± 0.86 |  | 20.8 ± 0.29 |
| RDW % | 12.23 ± 0.37 | 12.75 ± 0.44 | 12.44 ± 0.63 | 12.30 ± 0.55 | 12.44 ± 0.43 | 12.10 ± 0.88 | 13.08 ± 1.44 |  | 13.37 ± 0.8 |
| HDW Mmol/L | 1.62 ± 0.04 | 1.64 ± 0.06 | 1.65 ± 0.04 | 1.68 ± 0.06 | 1.66 ± 0.04 | 1.67 ± 0.12 | 2.01 ± 0.28** |  | 1.91 ± 0.10* |
| PLT x109/L | 969 ± 79 | 956 ± 114 | 1160 ± 172 | 915 ± 200 | 1033 ±94 | 971 ± 241 | 1171 ± 102 |  | 1135 ± 35 |
| MPV fl | 6.27 ± 0.50 | 6.58 ± 0.68 | 6.28 ± 0.58 | 6.46 ± 0.25 | 6.56 ± 0.73 | 7.16 ± 1.73 | 6.64 ± 1.35 |  | 6.33 ± 0.50 |
| Neutrophils % | 16.4 ± 2.6 | 15.8 ± 1.5 | 13.2 ± 4.4 | 16.0 ± 3.2 | 17.0 ± 2.4 | 16.8 ± 3.7 | 55.5 ± 14.1*** |  | 49.5 ± 7.4** |
| Lymphocytes % | 78.9 ± 3.2 | 79.1 ± 1.8 | 82.3 ± 5.1 | 79.5 ± 3.3 | 78.0 ± 2.8 | 77.3 ± 4.2 | 35.1 ± 16*** |  | 39.4 ± 9.4** |
| Monocytes % | 2.2 ± 0.5 | 2.7 ± 0.5 | 2.5 ± 0.4 | 2.2 ± 0.3 | 2.7 ± 0.5 | 3.8 ± 0.3** | 6.0 ± 0.7*** |  | 7.2 ± 0.5*** |
| Eosinophils % | 2.0 ± 0.8 | 1.8 ± 0.4 | 1.5 ± 0.6 | 1.7 ± 0.1 | 1.6 ± 0.6 | 1.4 ± 0.4 | 0.7 ± 0.1 |  | 0.8 ± 0.4 |
| LUC % | 0.5 ± 0.3 | 0.5 ± 0.1 | 0.4 ± 0.1 | 0.5 ± 0.1 | 0.6 ± 0.4 | 0.6 ± 0.1 | 2.6 ± 2.1 |  | 3.2 ± 1.8 |
| Basophils % | 0.03 ± 0.06 | 0.13 ± 0.05 | 0.09 ± 0.03 | 0.11 ± 0.03 | 0.08 ± 0.05 | 0.10 ± 0.09 | 0.08 ± 0.05 |  | 0.05 ± 0.00 |
| Reticulocytes % | 3.29 ± 0.16 | 3.27 ± 0.22 | 4.05 ± 0.25 | 3.65 ± 0.62 | 3.30 ± 0.61 | 1.74 ± 0.25** | 0.85 ± 0.11*** |  | 1.07 ± 0.12*** |
| Neutrophils x109/L | 1.36 ± 0.4 | 2.06 ± 0.3 | 1.53 ± 0.6 | 1.70 ± 0.2 | 2.25 ± 0.4 | 2.69 ± 0.7 | 10.1 ± 6.1** |  | 9.3 ± 4.4* |
| Lymphocytes x109/L | 6.52 ± 1.1 | 10.37 ± 1.5 | 9.42 ± 0.4 | 8.60 ± 1.7 | 10.54 ± 2.6 | 12.75 ± 4.1* | 5.59 ± 1.9 |  | 6.95 ± 2.3 |
| Monocytes x109/L | 0.19 ± 0.08 | 0.36 ± 0.09 | 0.28 ± 0.05 | 0.24 ± 0.06 | 0.38 ± 0.14 | 0.61 ± 0.15 | 1.08 ± 0.56** |  | 1.33 ± 0.55** |
| Eosinophils x109/L | 0.17 ± 0.05 | 0.23 ± 0.03 | 0.18 ± 0.08 | 0.18 ± 0.03 | 0.22 ± 0.09 | 0.21 ± 0.06 | 0.12 ± 0.04 |  | 0.15 ± 0.10 |
| LUC x109/L | 0.05 ± 0.04 | 0.07 ± 0.02 | 0.06 ± 0.01 | 0.05 ± 0.02 | 0.09 ± 0.07 | 0.11 ± 0.05 | 0.57 ± 0.56* |  | 0.60 ± 0.51* |
| Basophils x109/L | 0.00 ± 0.00 | 0.01 ± 0.01 | 0.01 ± 0.01 | 0.01 ± 0.01 | 0.01 ± 0.01 | 0.02 ± 0.02 | 0.01 ± 0.01 |  | 0.01 ± 0.01 |
| Reticulocytes x1012/L | 0.24 ± 0.02 | 0.25 ± 0.02 | 0.29 ± 0.02* | 0.26 ± 0.04 | 0.24 ± 0.04 | 0.13 ± 0.02** | 0.08 ± 0.01*** |  | 0.09 ± 0.01*** |

Values represent mean ± SD (n=4).  Blood samples were obtained at day 6/7 (24 or 48 hours after the last administration). For some animals blood was not available for evaluation. For the control group and the dose of 128 mg/kg (unscheduled autopsy the number of animals was n=3.

a)Unscheduled autopsy of dose group of 128 mg/kg at days 6/7 after treatment in view of poor condition of the animals.

Supplementary Table 3D Haematology in male rats at day 26 after 5 consecutive days of oral administration of Cu2CO3(OH)2 NPs.

| Cu2CO3(OH)2 NPs |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Dose | 0 mg/kg | 4 mg/kg | 8 mg/kg | 16 mg/kg | 32 mg/kg | 64 mg/kg |
| WBC x109/L | 10.50 ± 1.75 | 13.33 ± 2.62 | 10.76 ± 1.90 | 12.31 ± 1.47 | 11.93 ± 2.53 | 9.67 ± 1.38 |
| RBC x1012/L | 7.90 ± 1.14 | 7.94 ± 0.21 | 7.95 ± 0.34 | 7.85 ±0.26 | 7.83 ± 0.21 | 7.84 ± 0.15 |
| HgB Mmol/L | 8.40 ± 0.33 | 8.53 ± 0.36 | 8.55 ± 0.41 | 8.38 ± 0.26 | 8.28 ± 0.15 | 8.13 ± 0.33 |
| Hct L/L | 0.42 ± 0.02 | 0.41 ± 0.02 | 0.41 ± 0.02 | 0.41 ± 0.01 | 0.41 ± 0.01 | 0.39 ± 0.01 |
| MCV fl | 52 ±2 | 52 ±1 | 52 ±1 | 52 ±0 | 52 ±1 | 50 ± 2 |
| MCH fmol | 1.07 ± 0.05 | 1.07 ± 0.03 | 1.08 ± 0.03 | 1.06 ± 0.01 | 1.06 ± 0.02 | 1.04 ± 0.04 |
| MCHC Mmol/L | 20.4 ± 0.1 | 20.7 ± 0.3 | 20.8 ± 0.3 | 20.6 ± 0.2 | 20.4 ± 0.2 | 20.7 ± 0.2 |
| RDW % | 12.71 ± 0.40 | 13.24 ± 0.41 | 12.64 ± 0.39 | 13.23 ±0.81 | 13.76 ± 0.64 | 13.61 ± 0.68 |
| HDW Mmol/L | 1.79 ± 0.09 | 1.95 ± 0.13 | 1.91 ±0.04 | 1.90 ±0.09 | 1.98 ± 0.11 | 1.94 ±0.06 |
| PLT x109/L | 915 ± 69 | 717 ± 128 | 932 ± 143 | 981 ± 48 | 919 ± 74 | 939 ± 78 |
| MPV fl | 6.58 ± 0.53 | 6.93 ± 0.73 | 7.15 ± 1.01 | 6.71 ± 0.24 | 6.20 ± 0.35 | 6.67 ± 0.25 |
| Neutrophils % | 17.5 ± 5.2 | 19.7 ± 4.5 | 13.4 ± 2.2 | 18.7 ± 1.3 | 20.2 ± 7.0 | 17.7 ± 3.7 |
| Lymphocytes % | 79.0 ± 5.1 | 75.4 ± 3.3 | 82.6 ± 3.5 | 77.6 ± 1.7 | 75.2 ± 6.3 | 78.5 ± 3.4 |
| Monocytes % | 2.03 ± 0.41 | 3.06 ± 1.29 | 2.40 ± 1.31 | 2.11 ± 0.44 | 2.69 ± 0.86 | 1.76 ± 0.29 |
| Eosinophils % | 1.15 ± 0.25 | 1.40 ± 0.18 | 1.26 ± 0.27 | 1.38 ± 0.29 | 1.40 ± 0.44 | 1.60 ± 0.56 |
| LUC % | 0.2 ± 0.1 | 0.3 ± 0.2 | 0.3 ± 0.2 | 0.2 ± 0.0 | 0.4 ± 0.2 | 0.3 ± 0.2 |
| Basophils % | 0.11 ± 0.03 | 0.10 ± 0.04 | 0.06 ± 0.05 | 0.08 ± 0.03 | 0.10 ± 0.04 | 0.09 ± 0.02 |
| Reticulocytes % | 3.07 ± 0.28 | 3.05 ± 0.42 | 2.68 ± 0.35 | 3.38 ± 0.37 | 3.28 ± 0.40 | 3.31 ± 0.39 |
| Neutrophils x109/L | 1.86 ± 0.75 | 2.56 ± 0.45 | 1.47 ± 0.48 | 2.29 ± 0.24 | 2.29 ± 0.42 | 1.73 ± 0.51 |
| Lymphocytes x109/L | 8.27 ± 1.34 | 10.10 ± 2.29 | 8.84 ± 1.20 | 9.56 ± 1.18 | 9.08 ± 2.62 | 7.56 ± 0.91 |
| Monocytes x109/L | 0.22 ± 0.06 | 0.43 ± 0.22 | 0.27 ± 0.18 | 0.26 ± 0.09 | 0.34 ± 0.17 | 0.17 ± 0.05 |
| Eosinophils x109/L | 0.12 ± 0.01 | 0.19 ± 0.05 | 0.14 ± 0.06 | 0.17 ± 0.04 | 0.16 ± 0.04 | 0.15 ± 0.05 |
| LUC x109/L | 0.03 ± 0.01 | 0.05 ± 0.03 | 0.04 ± 0.02 | 0.02 ± 0.00 | 0.06 ± 0.04 | 0.03 ± 0.03 |
| Basophils x109/L | 0.01 ± 0.01 | 0.01 ± 0.01 | 0.01 ± 0.01 | 0.01 ± 0.01 | 0.01 ± 0.01 | 0.00 ± 0.00 |
| Reticulocytes x1012/L | 0.24 ± 0.02 | 0.24 ± 0.03 | 0.21 ± 0.03 | 0.27 ± 0.02 | 0.26 ± 0.03 | 0.26 ± 0.03 |

Values represent mean ± SD (n=4). Blood samples were obtained at day 26  (21 days after the last administration).For some animals blood was not available for evaluation. The number of animals is n=3 for the dose groups  of  1, 4 and 16 mg/kg b.w.

Supplementary Table 4 Bone marrow cellularity in male rats after 5 consecutive days of oral administration of CuO NPs and Cu2CO3(OH)2 NPs.

| CuO NPs |  |  |  |  |  |  |  |  | Pilot Study |  | Extra Study |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose | 0 mg/kg | 1 mg/kg | 2 mg/kg | 4 mg/kg | 8 mg/kg | 16 mg/kg | 32 mg/kg |  | 64 mg/kg |  | 512 mg/kga |
| Day 6 |  |  |  |  |  |  |  |  |  |  |  |
| Bone marrow cells Numberx109/L | 8.56 ± 2.67 | 9.45 ± 4.80 | 4.79 ± 2.99 | 12.78 ± 11.86 | 11.35 ± 8.16 | 8.19 ±2.45 | 7.94 ± 5.50 |  | 13.72 ± 13.26 (2) |  | 10.45 ± 4.97 |
| Day 26 |  |  |  |  |  |  |  |  |  |  |  |
| Bone marrow cells Numberx109/L | 12.91 ± 5.51 | 13.18 ± 6.91 (3) | 12.20 ± 6.53 | 11.19 ± 7.56 (3) | 6.11 ± 3.01 | 12.10 ± 2.44 (3) | 12.36 ± 2.01 |  | NP |  | NP |

| Cu2CO3(OH)2 NPs |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose | 0 mg/kg | 4 mg/kg | 8 mg/kg | 16 mg/kg | 32 mg/kg | 64 mg/kg | 128 mg/kg |  | 128 mg/kgb |
| Day 6 |  |  |  |  |  |  |  |  |  |
| Bone Marrow cells Number x109/L | 21.25 ± 6.72 | 22.90 ± 8.84 | 22.88 ± 2.27 | 18.80 ± 11.21 | 15.90 ± 3.80 | 14.68 ± 3.37 | 13.60 ± 2.72 |  | 18.09 ±2.09 |
| Day 26 |  |  |  |  |  |  |  |  |  |
| Bone Marrow cells Number x109/L | 16.71 ± 4.09 | 23.29 ± 6.18 | 18.86 ± 4.63 | 17.94 ± 8.94 | 18.82 ± 6.32 | 17.47 ± 4.09 | NP |  | NP |
| Erythroid BM cells (%) | 45.8 ± 4.3 |  |  |  |  |  | 16 ± 4.4 (3)*** |  | 22.8 ± 8.7** |
| Myeloid/ Lymphoid BM cells (%) | 54.2 ± 4.3 |  |  |  |  |  | 84 ± 4.4 (3)*** |  | 77.2 ± 8.7** |

Values represent mean ± SD  (n=4).

a) Animals with dose 512 mg/kg b.w. CuO NPs as extra group were treated without concurrent  control. For the dose of 64 mg/kg b.w. CuO NPs in the pilot study two (n=2) animals were evaluated. b)  Unscheduled autopsy of dose group of 128 mg/kg at days 6/7 after treatment in view of poor condition of the animals.

The number of animals per group is 4 (n=4) unless otherwise indicated in the table as for some animals Bone Marrow cells were  not available for evaluation. NP, not present. Significantly different compared to vehicle control treated animals :  ** p<0.01, *** P<0.001.

Supplementary Table 5A Clinical chemistry in male rats at day 6 after 5 consecutive days of oral administration of CuO NPs.

| CuO NPs |  |  |  |  |  |  |  |  | Pilot Study |  | Extra Study |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose | 0 mg/kg | 1 mg/kg | 2 mg/kg | 4 mg/kg | 8 mg/kg | 16 mg/kg | 32 mg/kg |  | 64 mg/kg |  | 512 mg/kga |
| TP g/L | 48 ± 2 | 45 ± 2 | 47 ± 1 | 47 ± 1 | 47 ± 0.5 | 46 ± 1 | 44 ± 2 |  | 46 ± 0.4 |  | 52 ± 3 |
| ALB g/L | 13.3 ± 0.6 | 12.7 ± 0.5 | 12.9 ± 0.4 | 13.1 ± 0.3 | 13.2 ± 0.2 | 12.7 ± 0.2 | 12.5 ± 0.4 |  | 12.9 ± 0.2 |  | 13.7 ± 0.9 |
| ALP IU/L | 327 ± 27 | 301 ± 33 | 268 ± 10* | 277 ± 9* | 338 ± 14 | 283 ± 10* | 262 ± 29* |  | 244 ± 13* |  | 176 ± 76 |
| ALT IU/L | 51 ± 6 | 51 ± 5 | 45 ± 2 | 47 ± 3 | 49 ± 4 | 47 ± 1 | 52 ± 4 |  | 53 ± 1 |  | 704 ± 451 |
| AST IU/L | 59 ± 2 | 62 ± 9 | 55 ± 2 | 53 ± 4 | 58 ± 4 | 55 ± 4 | 78 ± 7** |  | 84 ± 0.4** |  | 899 ± 653 |
| GGT U/L | 0.48 ± 0.3 | 0.53 ± 0.4 | 0.75 ± 0.6 (3) <DL(1) | 0.51 ± 0.3 (3) <DL(1) | 0.30 ± 0.2 (2) <DL(2) | 0.35 ± 0.2 (3) <DL(1) | 0.59 (1) <DL(2) |  | 0.16 + 0.1 |  | 0.26 ± 0.2 (3) |
| LDH IU/L | 573 ± 175 | 399 ± 78* | 340 ± 24 | 435 ± 222 | 622 ± 3.26 | 390 ± 110 | 797 ± 812 |  | 1788 ± 64** |  | 4452 ± 1622 |
| CHOL mmol/L | 1.25 ± 0.05 | 1.25 ± 0.1 | 1.24 ± 0.1 | 1.19 ± 0.1 | 1.22 ± 0.1 | 1.28 ± 0.03 | 1.21± 0.1 |  | 1.20 ± 0.02 |  | 1.64 ± 0.3 |
| TG mmol/L | 1.13 ± 0.21 | 0.97 ± 0.37 | 1.44 ± 0.24 | 1.28 ± 0.37 | 1.21 ± 0.21 | 1.10 ± 0.31 | 0.91 ± 0.29 |  | 1.26 ± 0.45 |  | 1.11 ± 0.4 |
| CRE µmol/L | 14.0 ± 1.52 | 14.2 ± 2.2 | 15.3 ± 1.1 | 14.1 ± 2.0 | 15.2 ± 2.2 | 15.1 ± 1.4 | 15.2 ± 2.4 |  | 12.4 ± 0.5 |  | 28.7 ± 6.4 |
| GLU mmol/L | 10.8 ± 0.8 | 10.6 ± 1.5 | 11.1 ± 0.2 | 11.8 ± 0.8 | 11.2 ± 0.6 | 11.4 ± 0.4 | 11.2± 1.7 |  | 10.7 ± 0.5 |  | 8.21 ± 1.2 |
| K mmol/L | 4.5 ± 0.3 | 4.5 ± 0.2 | 5.1 ± 0.2 | 4.6 ± 0.2 | 4.9 ± 0.3 | 4.7 ± 0.2 | 4.6 ± 0.4 |  | 4.3 ± 0.01 |  | 5.0 ± 0.2 |
| Ca mmol/L | 2.57 ± 0.07 | 2.49 ± 0.08 | 2.50 ± 0.04 | 2.51 ± 0.04 | 2.57 ± 0.02 | 2.49 ± 0.03 | 2.42 ± 0.04 |  | 2.46 ± 0.00 |  | 2.4 ± 0.07 |
| Cl mmol/L | 99.3 ± 2.8 | 99.5 ± 1.2 | 99.4 ± 1.0 | 98.4 ± 0.4 | 97.5 ± 1.2 | 97.4 ± 0.8 | 98.98 ± 1.7 |  | 99 ± 1.2 |  | 103 ± 1.9 |
| Fe µmol/L | 32.3 ± 1.9 | 33.2 ± 1.2 | 31.4 ± 2.6 | 31.9 ± 3.7 | 37.2 ± 6.1 | 37.4 ± 5.9 | 56.3 ± 18.2* |  | 68.7 ± 7.7** |  | 18.7 ± 8.0 |
| Na mmol/L | 142 ± 3.0 | 141 ± 0.8 | 139 ± 0.4 | 140 ± 0.7 | 141 ± 0.4 | 139 ± 0.5 | 140 ± 2.1 |  | 142 ± 0.7 |  | 143 ± 2.8 |
| Urea mmol/L | 5.7 ± 0.6 | 5.4 ± 0.7 | 5.1 ± 0.4 | 5.8 ± 0.2 | 6.3 ± 0.5 | 5.3 ± 0.1 | 5.4 ± 0.7 |  | 5.5 ± 0.7 |  | 6.6 ± 0.7 |
| Uric Acid | 41 ± 3.1 | 43 ± 14 | 44 ± 1.4 | 34 ± 4.3 | 44 ± 14 | 39 ± 3.9 | 60 ± 3.1** |  | 43 ± 6.1 |  | 74 ± 14 |
| TBAX µmol/L | 41 ± 12 | 62 ± 71 | 25 ± 12 | 31 ± 9 | 24 ± 13 | 21 ± 18 | 35 ± 8 |  | 8 ± 1* |  | nd |
| TBIL µmol/L | 8.3 ± 1.2 | 7.8 ± 0.9 | 8.0 ± 0.6 | 7.1 ± 0.2 | 8.5 ± 0.2 | 7.4 ± 0.8 | 9.5 ± 0.2 |  | 7.1 ± 1.5 |  | 6.6 ± 2.5 |
| ROM IU/L | 233 ± 26 | 216 ± 38 | 232 ± 14 | 246 ± 8 | 231 ± 21 | 230 ± 13 | 224 ± 50 |  | 265 ± 28 |  | 342 ± 75 |
| SHP µmol/L | 310 ± 19 | 297 ± 22 | 290 ± 28 | 295 ± 21 | 291 ± 30 | 269 ± 14* | 283 ± 9 |  | 224 ± 19* |  | 111 ± 45 |

Values represent mean ± SD. Blood was obtained at day 6 (24 hours after the last administration).

Abbreviations: ALB, albumin; ALP, alkaline phosphatase, ALT, alanine aminotransferase; AST, aspartate aminotransferase; BAP, biological anto-oxidant potential; Ca, calcium; Cl, chloride; ; CHOL, cholesterol; CRE, creatinine; Fe, iron; GGT, gamma glutamyltransferase; GLU, glucose; K, potassium; LDH, lactate dehydrogenase; Na, sodium; ROM, reactive oxygen metabolites; SHP, plasmatic thiol groups; TBAX, total bile acids; TBIL, total bilirubin; TG, triglycerides;  TP, total protein; TTT, total thiols.

a) Animals with dose 512 mg/kg b.w. CuO NPs as extra group were treated without concurrent  control. For the dose of 64 mg/kg b.w. CuO NPs in the pilot study two (n=2) animals were evaluated. In other dose groups the number of animals is n=4. Significant differences with non treated control animals *p<0.05, **p<0.01 (ANOVA).

Supplementary Table 5B Clinical chemistry in male rats at day 26 after 5 consecutive days of oral administration of CuO-NP.

| CuO NPs |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Dose | 0 mg/kg | 1 mg/kg | 2 mg/kg | 4 mg/kg | 8 mg/kg | 16 mg/kg | 32 mg/kg |
| TP g/L | 49 ± 1 | 49 ± 1 | 49 ± 2 | 50 ± 1 (3) <DL(1) | 51 ± 1 | 50 ± 1 | 52 ± 1 |
| ALB g/L | 13.6 ± 0.2 | 13.5 ± 0.6 | 13.2 ± 0.3 | 13.6 ± 0.3 (3) <DL(1) | 14.1 ± 0.3 | 13.8 ± 0.3 | 13.8 ± 0.3 |
| ALP IU/L | 276 ± 19 | 290 ± 21 | 232 ± 19* | 209 ± 62 | 274 ± 30 | 241 ± 29 | 236 ± 44 |
| ALT IU/L | 49 ± 4.9 | 52 ± 4.0 | 46 ± 4.1 | 43 ± 5.4 | 50 ± 5.9 | 51 ± 2.1 | 46 ± 2.0 |
| AST IU/L | 64 ± 3.7 | 70 ± 6.7 | 62 ± 1.4 | 63 ± 4.1 | 66 ± 3.7 | 65 ± 4.4 | 68 ± 6.0 |
| GGT U/L | 0.44 ± 0.2 (2) <DL(2) | 0.51 ± 0.3 (3) <DL(1) | 0.15 ± 0.1 | 0.27 ± 0.1 | 0.73 ± 0.3 (2) <DL(2) | 0.26 ± 0.1 (3) <DL(1) | 0.54 ± 0.1 (2) <DL(2) |
| LDH IU/L | 635 ± 129 | 634 ± 316 | 585 ± 223 | 694 ± 156 | 547 ± 242 | 573 ± 205 | 822 ± 131 |
| CHOL mmol/L | 1.26 ± 0.06 | 1.26 ± 0..02 | 1.26 ± 0.09 | 1.26 ± 0.10 | 1.24 ± 0.05 | 1.30 ± 0.10 | 1.40 ± 0.20 |
| TG mmol/L | 1.21 ± 0.15 | 1.17 ± 0.20 | 1.27 ± 0.30 | 1.22 ± 0.18 (3) <DL()1) | 1.49 ± 0.20 | 1.08 ± 0.22 | 1.41 ± 0.26 |
| CRE µmol/L | 17.5 ± 1.1 | 18.5 ± 2.6 | 19.2 ± 1.2 | 20.9 ± 1.8 (3) <DL(1) | 20.4 ± 3.4 | 19.9 ± 2.3 | 22.9 ± 5.4 |
| GLU mmol/L | 10.8 ± 1.2 | 10.2 ± 0.8 | 10.2 ± 0.3 | 10.6 ± 0.7 | 10.4 ± 0.6 | 10.1 ± 1.1 | 10.9 ± 0.3 |
| K mmol/L | 4.8 ± 0.1 | 4.8 ± 0.2 | 5.0 ± 0.1 | 4.8 ± 0.2 | 4.9 ± 0.1 | 4.9 ± 0.3 | 4.8 ± 0.3 |
| Ca mmol/L | 2.58 ± 0.06 | 2.49 ± 0.05 | 2.53 ± 0.05 | 2.70 ± 0.29 | 2.52 ± 0.02 | 2.55 ± 0.06 | 2.54 ± 0.06 |
| Cl mmol/L | 98 ± 0.7 | 100 ± 1.2 | 99 ± 0.5 | 98 ± 0.8 (3) | 98 ± 1.3 | 98 ± 0.8 | 99 ± 1.0 |
| Fe µmol/L | 36.3 ± 1.9 | 33.4 ± 2.1 | 35.4 ± 1.4 | 33.8 ± 5.7 | 35.3 ± 2.0 | 36.7 ± 1.4 | 40.1 ± 4.2 |
| Na mmol/L | 142 ± 0.7 | 141 ± 1.0 | 141 ± 0.6 | 140 ± 0.3 (3) | 141 ± 0.4 | 141 ± 1.3 | 142 ± 1.5 |
| Urea mmol/l | 6.2 ± 0.2 | 6.1 ± 0.3 | 5.8 ± 0.3 | 6.8 ± 1.7 | 7.1 ± 0.3 | 6.1 ± 0.4 | 6.6 ± 1.6 |
| Uric Acid | 43 ± 10.4 | 39 ± 8.2 | 43 ± 5.3 | 49 ± 19.8 | 41 ± 4.5 | 47 ± 10.0 | 45 ± 7.2 |
| TBAX µmol/L | 43 ± 5 | 26 ± 17 | 33 ± 13 | 34 ± 17 | 50 ± 13 | 45 ± 18 | 31 ± 12 |
| TBIL µmol/L | 7.1 ± 1.0 | 8.4 ± 1.0 | 7.8 ± 0.8 | 9.7 ± 3.6 | 7.5 ± 0.7 | 8.3 ± 1.0 | 7.7 ± 0.9 |
| ROM IU/L | 265 ± 28 | 258 ± 7 | 255 ± 12 | 268 ± 34 | 266 ± 16 | 260 ± 14 | 288 ± 35 |
| SHP µmol/L | 260 ± 17 | 272 ± 11 | 233 ± 11 | 216 ± 54 | 276 ± 13 | 240 ± 9 | 244 ± 17 |

Values represent mean ± SD. Blood was obtained at day 26 (21 days after the last administration). Abbreviations: ALB, albumin; ALP, alkaline phosphatase, ALT, alanine aminotransferase; AST, aspartate aminotransferase; BAP, biological anto-oxidant potential; Ca, calcium; Cl, chloride; ; CHOL, cholesterol; CRE, creatinine; Fe, iron; GGT, gamma glutamyltransferase; GLU, glucose; K, potassium; LDH, lactate dehydrogenase; Na, sodium; ROM, reactive oxygen metabolites; SHP, plasmatic thiol groups; TBAX, total bile acids; TBIL, total bilirubin; TG, triglycerides;  TP, total protein; TTT, total thiols.   DL, detection limit.

Number of animals n=4 unless indicated otherwise within brackets. Significant differences with non treated control animals *p<0.05, **p<0.01 (ANOVA).

Supplementary Table 5C Clinical chemistry in male rats at day 6 after 5 consecutive days of oral administration of Cu2CO3(OH)2 NPs.

| Cu2CO3(OH)2 NPs |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose | 0 mg/kg | 4 mg/kg | 8 mg/kg | 16 mg/kg | 32 mg/kg | 64 mg/kg | 128 mg/kg |  | 128 mg/kga |
| TP g/L | 55.4 ± 0.6 | 55.9 ± 0.8 | 56.5 ± 1.2 | 54.7 ± 2.2 | 53.5 ± 1.4 | 50.3 ± 2.5* | 55.8 ± 3.7 (3) |  | 52.1 ± 4.3 (3) |
| ALB g/L | 15.7 ± 0.6 | 16.0 ± 0.5 | 15.9 ± 0.7 | 16.1 ± 0.8 | 15.0 ± 0.7 | 14.2 ± 1.5 | 15.9 ± 1.8 (3) |  | 14.5 ± 0.9 (3) |
| ALP IU/L | 222 ± 35 | 256 ± 20 | 208 ± 16 | 266 ± 48 | 238 ± 19 | 247 ± 51 | 80 ± 21** |  | 116 ± 18** |
| ALT IU/L | 54 ± 2 | 59 ± 4 | 57 ± 13 | 58 ± 10 | 60 ± 14 | 310 ± 94** | 409 ± 360 |  | 612 ± 186** |
| AST IU/L | 93 ± 9 | 96 ± 8 | 97 ± 15 | 101 ± 10 | 113 ± 19 | 438 ± 110** | 1224 ± 545* |  | 1771 ± 1122* |
| GGT U/L | 0.36 ± 0.2 (3) <DL(1) | 0.50 ± 0.1 (2) <DL(2) | 0.35 ± 0.1 (2) <DL(1) | 047 ± 0.3 (2) <DL(2) | 0.55 (1) <DL(2) | 0.32 ± 0.2 (3) <DL(1) | 0.27 ± 0.2 (3) <DL(1) |  | 7.1 (1) |
| LDH IU/L | 2229 ± 468 | 1796 ± 455 | 2556 ± 656 | 2229 ± 710 | 2754 ± 462 | 3139 ± 1726 | 9406 ± 4903* |  | 3667 ± 1173 |
| FFA Mmol/L | 0.17 ± 0.04 | 0.20 ± 0.1 | 0.19 ± 0.03 | 0.19 ± 0.04 | 0.25 ± 0.04 | 0.42 ± 0.2** | 0.65 ± 0.1** |  | 0.62 ± 0.2** |
| CHOL mmol/L | 1.21 ± 0.1 | 1.40 ± 0.2 | 1.32 ± 0.1 | 1.42 ± 0.2 | 1.23 ± 0.2 | 1.88 ± 0.4* | 1.58 ± 0.4 |  | 2.44 ± 0.5** |
| TG mmol/L | 1.70 ± 0.44 | 1.71 ± 0.37 | 2.45 ± 0.47 | 1.97 ± 0.24 | 1.84 ± 0.29 | 1.59 ± 0.6 | 1.23 ± 0.5 |  | 1.06 ± 0.28 |
| CRE µmol/L | 22.6 ± 2.2 | 21.7 ± 3.5 | 23.7 ± 0.9 | 24.2 ± 2.4 | 25.0 ± 3.1 | 23.0 ± 3.2 | 190 ± 110 (3)** |  | 56.2 ± 49 |
| GLU mmol/L | 11.8 ± 0.8 | 11.0 ± 0.5 | 11.6 ± 1.2 | 11.6 ± 1.1 | 10.8 ± 0.3 | 10.2 ± 1.3 | 7.1 ± 2.0** |  | 9.6 = 4.0 |
| K mmol/L | 4.81 ± 0.2 | 4.94 ± 0.4 | 4.90 ± 0.1 | 4.89 ± 0.4 | 5.00 ± 0.2 | 5.24 ± 0.5 | 6.10 ± 0.6 (3)* |  | 5.59 ± 0.2 (3)* |
| Ca mmol/L | 2.49 ± 0.04 | 2.60 ± 0.04* | 2.57 ± 0.03* | 2.59 ± 0.06 | 2.55 ± 0.01* | 2.53 ± 0.02 | 2.56 ± 0.18 |  | 2.53 ± 0.15 |
| Cl mmol/L | 101 ± 1.5 | 100 ± 0.4 | 101 ± 0.9 | 100 ± 2 | 101 ± 0.7 | 104 ± 0.8* | 99 ± 0.9 (3) |  | 102 ± 1.5 (3) |
| Fe µmol/L | 30.9 ± 2 | 36.3 ± 4 | 39.7 ± 6* | 51.3 ± 11* | 64.8 ± 19* | 43.3 ± 24 | 66.5 ± 23* |  | 51.6 ± 33 |
| Na mmol/L | 142 ± 0.5 | 141 ± 0.5 | 142 ± 2.0 | 143 ± 3.3 | 142 ± 0.6 | 143 ± 1.8 | 137 ± 3.7 (3) |  | 140 ± 2.4 (3) |
| Urea mmol/l | 6.06 ± 1.0 | 6.44 ± 0.7 | 5.78 ± 1.2 | 6.48 ± 0.6 | 6.24 ± 0.7 | 5.47 ± 0.6 | 25.8 ± 14.5 |  | 13.3 ± 5.3 |
| Uric Acid | 69 ± 27 | 53 ± 4 | 74 ± 12 | 50 ± 5 | 66 ± 7 | 55 ± 6 | 151 ± 49* |  | 119 ± 58 |
| TBIL µmol/L | 5.96 ± 0.19 | 5.33 ± 0.62 | 5.55 ± 0.66 | 5.75 ± 0.5 | 6.38 ± 0.75 | 6.11 ± 0.4 | 13.73 ± 9.66 |  | 12.92 ± 7.65 |
| ROM IU/L | 292 ± 30 | 280 ± 22 | 256 ± 14 | 261 ± 8 | 246 ±16 | 332 ± 35 | 406 ± 189 |  | 360 ± 47 |
| SHP µmol/L | 323 ± 41 | 373 ± 27 | 335 ± 16 | 354 ± 20 | 328 ± 13 | 277 ± 36 | 197 ± 160 |  | 148 ± 112* |

Values represent mean ± SD with n=4 unless indicated otherwise within brackets. Blood was obtained at day 6 (24 hours after the last administration).

Abbreviations: ALB, albumin; ALP, alkaline phosphatase, ALT, alanine aminotransferase; AST, aspartate aminotransferase; BAP, biological anto-oxidant potential; Ca, calcium; Cl, chloride; ; CHOL, cholesterol; CRE, creatinine; Fe, iron; GGT, gamma glutamyltransferase; GLU, glucose; K, potassium; LDH, lactate dehydrogenase; Na, sodium; ROM, reactive oxygen metabolites; SHP, plasmatic thiol groups; TBAX, total bile acids; TBIL, total bilirubin; TG, triglycerides;  TP, total protein; TTT, total thiols.  DL, detection limit.

a)Unscheduled autopsy of dose group of 128 mg/kg at days 6/7 after treatment in view of poor condition of the animals.

Significant differences with non treated control animals *p<0.05, **p<0.01 (ANOVA).

Supplementary Table 5D Clinical chemistry in male rats at day 26 after 5 consecutive days of oral administration of Cu2CO3(OH)2 NPs.

| Cu2CO3(OH)2 NPs |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Dose | 0 mg/kg | 4 mg/kg | 8 mg/kg | 16 mg/kg | 32 mg/kg | 64 mg/kg |
| TP g/L | 58.6 ± 2.4 | 56.9 ± 2.7 | 56.4 ± 3.0 | 59.4 ± 1.7 | 57.5 ± 1.9 | 57.1 ± 1.6 |
| ALB g/L | 16.3 ± 0.7 | 15.5 ± 1.0 | 15.3 ± 1.1 | 16.8 ± 0.2 | 16.6 ± 0.5 | 16.0 ± 1.3 |
| ALP IU/L | 205 ± 18 | 188 ± 24 | 178 ± 31 | 229 ± 40 | 197 ± 28 | 256 ± 39 |
| ALT IU/L | 63.7 ± 4.7 | 70.4 ± 9.6 | 48.5 ± 3.8** | 69.3 ± 13.1 | 66.0 ± 8.3 | 87.2 ± 32.3 |
| AST IU/L | 120 ± 7 | 110 ± 9 | 92 ± 6** | 121 ± 10 | 112 ± 5 | 153 ± 55 |
| GGT U/L | 0.71 (1) <DL(3) | 0.49 ± 0.0 (2) <DL(1) | 1.11 (1) <DL(3) | 0.44 (1) <DL(3) | 0.67 ± 0.3 (2) <DL(2) | 0.69 ± 0.2 (3) <DL(1) |
| LDH IU/L | 3271 ± 548 | 2108 ± 333* | 1878 ± 455* | 2254 ± 688 | 2217 ± 657 | 2488 ± 636 |
| CHOL mmol/L | 1.32 ± 0.2 | 1.39 ± 0.1 | 1.47 ± 0.1 | 1.40 ± 0.1 | 1.14 ± 0.1 | 1.28 ± 0.1 |
| TG mmol/L | 2.20 ± 0.89 | 2.58 ± 0.80 | 2.27 ± 0.65 | 2.84 ± 1.03 | 2.19 ± 0.91 | 1.80 ± 0.28 |
| CRE µmol/L | 27.2 ± 2.1 | 28.4 ± 1.8 | 28.0 ± 2.3 | 31.6 ± 2.7 | 29.4 ± 2.3 | 31.2 ± 1.5* |
| GLU mmol/L | 11.3 ± 1.8 | 10.8 ± 1.3 | 13.8 ± 2.5 | 11.4 ± 0.8 | 11.1 ± 0.7 | 12.3 ± 1.1 |
| K mmol/L | 4.84 ± 0.3 | 5.08 ± 0.3 | 4.80 ± 0.3 | 4.94 ± 0.4 | 4.86 ± 0.3 | 4.74 ± 0.1 |
| Ca mmol/L | 2.50 ± 0.03 | 2.55 ± 0.05 | 2.49 ± 0.07 | 2.50 ± 0.04 | 2.53 ± 0.05 | 2.47 ± 0.06 |
| Cl mmol/L | 102 ± 1.3 | 102 ± 1.1 | 102 ± 1.4 | 101 ± 1.5 | 102 ± 1.7 | 102 ± 1.0 |
| Fe µmol/L | 30.5 ± 3.9 | 31.1 ± 7.7 | 29.9 ± 3.0 | 29.5 ± 4.2 | 30.8 ± 5.9 | 29.0 ± 3.8 |
| Na mmol/L | 144 ± 1.1 | 143 ± 1.9 | 142 ± 1.5 | 142 ± 1.4 | 144 ± 1.0 | 143 ± 1.6 |
| Urea mmol/l | 7.13 ± 0.7 | 7.28 ± 0.5 | 6.49 ± 0.9 | 7.56 ± 0.6 | 6.59 ± 0.8 | 7.04 ± 0.8 |
| Uric Acid | 48 ± 3 | 45 ±5 (3) <DL(1) | 51 ± 6 | 62 ± 12 | 49 ± 5 | 54 ± 12 |
| TBIL µmol/L | 5.38 ± 0.28 | 5.30 ± 0.69 | 5.73 ± 0.83 | 6.12 ± 0.17** | 5.22 ± 0.77 | 5.01 ± 0.71 |
| Zn µg/dL | 119 ± 3 | 136 ± 6 | 124 ± 9 | 125 ± 3 | 132 ± 7 | 114 ± 10 |
| ROM IU/L | 297 ± 16 | 272 ± 23 | 274 ± 26 | 304 ± 22 | 279 ± 11 | 289 ± 23 |
| SHP µmol/L | 349 ± 6 | 324 ± 21 | 331 ± 25 | 327 ± 22 | 328 ± 17 | 340 ± 39 |

Values represent mean ± SD with n=4 unless indicated otherwise within brackets. Blood was obtained at day 26 (21 days after the last administration). Abbreviations: ALB, albumin; ALP, alkaline phosphatase, ALT, alanine aminotransferase; AST, aspartate aminotransferase; BAP, biological anti-oxidant potential; Ca, calcium; Cl, chloride; ; CHOL, cholesterol; CRE, creatinine; Fe, iron; GGT, gamma glutamyltransferase; GLU, glucose; K, potassium; LDH, lactate dehydrogenase; Na, sodium; ROM, reactive oxygen metabolites; SHP, plasmatic thiol groups; TBAX, total bile acids; TBIL, total bilirubin; TG, triglycerides;  TP, total protein; TTT, total thiols.  DL, detection limit.

Significant differences with non treated control animals *p<0.05, **p<0.01 (ANOVA).

Supplementary Table 6 Histopathology in male rats at day 6 and day 26  after 5 consecutive days of oral administration of CuO-NP and Cu2CO3(OH)2 NPs .

| Gastro-intestinal system |  | Cu2CO3(OH)2-NP |  |  |  |  |  |  |  |  |  | CuO-NP |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose level (mg/kg): | 0 |  | 64 |  | 128 |  | 128 |  | 0 |  | 64 | 512 |
| Autopsy day | Day 6 |  | Day 6 |  | Day 6 |  | Day 7 |  | Day 26 |  | Day 26 | Day 6 |
| STOMACH a | 4 |  | 4 |  | 4 |  | 4 |  | 4 |  | 4 | 4 |
| Inflammation |  |  |  |  |  |  |  |  |  |  |  |  |
| Minimal | 2 |  | - |  | 1 |  | 1 |  | 1 |  | - | - |
| Slight | - |  | - |  | 3 |  | 3 |  | - |  | 2 | 1 |
| Moderate | - |  | 4 |  | - |  | - |  | - |  | 2 | 3 |
| DUODENUM a | 4 |  | 3 |  | 4 |  | 4 |  | 4 |  | 4 | 4 |
| Apoptosis |  |  |  |  |  |  |  |  |  |  |  |  |
| Slight | - |  | - |  | - |  | 2 |  | - |  | - | - |
| Moderate | - |  | - |  | - |  | 1 |  | - |  | - | - |
| ILEUM a | 4 |  | 4 |  | 4 |  | 4 |  | 4 |  | 4 | 4 |
| Apoptosis |  |  |  |  |  |  |  |  |  |  |  |  |
| Moderate | - |  | - |  | - |  | 1 |  | - |  | - | 4 |
| CECUM | 4 |  | 4 |  | 4 |  | 4 |  | 4 |  | 4 | 4 |
| Ulceration/erosion |  |  |  |  |  |  |  |  |  |  |  |  |
| Minimal | - |  | - |  | - |  | 1 |  | - |  | - | - |
| Apoptosis |  |  |  |  |  |  |  |  |  |  |  |  |
| Moderate | - |  | - |  | - |  | 1 |  | - |  | - | - |
| COLON | 4 |  | 4 |  | 4 |  | 4 |  | 4 |  | 4 | 4 |
| Ulceration/erosion |  |  |  |  |  |  |  |  |  |  |  |  |
| Slight | - |  | - |  | 2 |  | 1 |  | - |  | - | 4 |
| Edema |  |  |  |  |  |  |  |  |  |  |  |  |
| Slight | - |  | - |  | 1 |  | 1 |  | - |  | - | - |
| RECTUM a | 4 |  | 4 |  | 4 |  | 4 |  | 4 |  | 4 | 4 |
| Inflammation |  |  |  |  |  |  |  |  |  |  |  |  |
| Minimal | - |  | - |  | 1 |  | - |  | - |  | - | - |
| Slight | - |  | - |  | - |  | 2 |  | - |  | - | - |
| Edema |  |  |  |  |  |  |  |  |  |  |  |  |
| Minimal | - |  | - |  | 1 |  | - |  | - |  | - | - |
| Slight | - |  | - |  | - |  | 1 |  | - |  | - | - |
| Ulceration/erosion |  |  |  |  |  |  |  |  |  |  |  |  |
| Minimal | - |  | - |  | - |  | 1 |  | - |  | - | - |
| Slight | - |  | - |  | - |  | 1 |  | - |  | - | - |
| Moderate | - |  | - |  | - |  | 1 |  | - |  | - | - |

a  =  Number of tissues examined from each group.

| Other organs |  | Cu2CO3(OH)2-NP |  |  |  |  |  |  |  |  |  | CuO-NP |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Dose level (mg/kg): | 0 |  | 64 |  | 128 |  | 128 |  | 0 |  | 64 | 512 |
| Autopsy day | Day 6 |  | Day 6 |  | Day 6 |  | Day 7 |  | Day 26 |  | Day 26 | Day 6 |
| LIVER a | 4 |  | 4 |  | 4 |  | 4 |  | 4 |  | 4 | 4 |
| Inflammation |  |  |  |  |  |  |  |  |  |  |  |  |
| Slight | - |  | 2 |  | - |  | 1 |  | - |  | - | - |
| Moderate | - |  | 1 |  | 1 |  | 2 |  | - |  | - | 1 |
| Marked | - |  | - |  | - |  | - |  | - |  | - | 1 |
| Kupffer cell hypertrophy /hyperplasia |  |  |  |  |  |  |  |  |  |  |  |  |
| Slight | - |  | - |  | 1 |  | - |  | - |  | - | 2 |
| Moderate | - |  | - |  | 1 |  | 2 |  | - |  | - | - |
| Hypertrophy |  |  |  |  |  |  |  |  |  |  |  |  |
| Minimal | - |  | - |  | - |  | 1 |  | - |  | - | 2 |
| Slight | - |  | 1 |  | 2 |  | 2 |  | - |  | - | - |
| Moderate | - |  | 1 |  | - |  | 1 |  | - |  | - | 1 |
| Necrosis |  |  |  |  |  |  |  |  |  |  |  |  |
| Minimal | - |  | 1 |  | - |  | - |  | - |  | - | - |
| Slight | - |  | - |  | 1 |  | - |  | - |  | - | 1 |
| Moderate | - |  | - |  | - |  | - |  | - |  | - | 1 |
| Marked | - |  | - |  | - |  | - |  | - |  | - | 1 |
| Single cell necrosis |  |  |  |  |  |  |  |  |  |  |  |  |
| Minimal | - |  | 1 |  | 1 |  | - |  | - |  | 1 | 1 |
| Slight | - |  | 2 |  | 1 |  | 1 |  | - |  | - | - |
| Moderate | - |  | 1 |  | 2 |  | 1 |  | - |  | - | 1 |
| Marked | - |  | - |  | - |  | 1 |  | - |  | - | 1 |
| Vacuolation |  |  |  |  |  |  |  |  |  |  |  |  |
| Slight | - |  | - |  | 3 |  | 1 |  | - |  | - | - |
| SPLEEN a | 4 |  | 4 |  | 4 |  | 4 |  | 4 |  | 4 | 4 |
| Lymphoid atrophy |  |  |  |  |  |  |  |  |  |  |  |  |
| Minimal | - |  | - |  | 1 |  | 2 |  | - |  | - | - |
| Slight | - |  | - |  | 1 |  | - |  | - |  | - | - |
| THYMUS | 4 |  | 4 |  | 4 |  | 2 |  | 4 |  | 4 | 4 |
| Lymphoid atrophy |  |  |  |  |  |  |  |  |  |  |  |  |
| Moderate | - |  | - |  | - |  | 2 |  | - |  | - | - |
| KIDNEY a | 4 |  | 4 |  | 4 |  | 4 |  | 4 |  | 4 | 4 |
| Necrosis |  |  |  |  |  |  |  |  |  |  |  |  |
| Marked | - |  | - |  | 2 |  | - |  | - |  | - | - |
| Hyaline casts |  |  |  |  |  |  |  |  |  |  |  |  |
| Minimal | - |  | - |  | - |  | - |  | - |  | 1 | - |
| Slight | - |  | - |  | - |  | 1 |  | - |  | - | - |
| Marked | - |  | - |  | 2 |  | - |  | - |  | - | - |
| Degeneration/regeneration |  |  |  |  |  |  |  |  |  |  |  |  |
| Moderate | - |  | - |  | - |  | 2 |  | - |  | - | - |
| Inclusions |  |  |  |  |  |  |  |  |  |  |  |  |
| Moderate | - |  | - |  | - |  | 2 |  | - |  | - | - |
| TESTIS LEFT a | 4 |  | 4 |  | 4 |  | 4 |  | 4 |  | 4 | 4 |
| Multinucleated giant cells |  |  |  |  |  |  |  |  |  |  |  |  |
| Slight | - |  | - |  | 1 |  | - |  | - |  | - | - |
| Degeneration germ cells |  |  |  |  |  |  |  |  |  |  |  |  |
| Moderate | - |  | - |  | 1 |  | - |  | - |  | - | - |
| Retention |  |  |  |  |  |  |  |  |  |  |  |  |
| Marked | - |  | - |  | 1 |  | - |  | - |  | - | - |
| SEMINAL VESICLES a | 1 |  | - |  | 4 |  | 4 |  | - |  | - | - |
| Decreased fluid |  |  |  |  |  |  |  |  |  |  |  |  |
| Minimal | - |  | - |  | - |  | 1 |  | - |  | - | - |
| Slight | - |  | - |  | 4 |  | 2 |  | - |  | - | -- |
| Moderate | - |  | - |  | - |  | 1 |  | - |  | - | - |
| BONE MARROW FEMUR a | 4 |  | 4 |  | 4 |  | 4 |  | 4 |  | 4 | 3 |
| Increased myeloid/ decreased erythroid |  |  |  |  |  |  |  |  |  |  |  |  |
| Minimal | - |  | - |  | 2 |  | - |  | - |  | - | - |
| Slight | - |  | - |  | - |  | 3 |  | - |  | - | 1 |
| Moderate | - |  | - |  | 1 |  | - |  | - |  | - | - |

a  =  Number of tissues examined from each group.

Supplementary Table 7  Bench mark dose calculations for effects after oral CuO nanoparticles exposure for 5 consecutive days.

| Parameter | BMDexp | BMDhill | BMDavg | BMDlow | BMDhigh | ratio |
| --- | --- | --- | --- | --- | --- | --- |
| Body weight | 58a | 58 | 58 | 28 | infinitive | No value |
| Liver weight | 26.4 | 26.4 | 26.4 | 1.2 | 30.1 | 25.1 |
| AST | 26.2 | 26.2 | 26.2 | 16.1 | 27.0 | 1.7 |
| ALP05b | 0.41 | 0.41 | 0.41 | 0 | 27.7 | No value |
| ALP10 | 6.11 | 5.97 | 6.04 | 0.0006 | 419.9 | 699833 |
| LDP05 | 26.6 | 26.9 | 26.8 | 0.49 | infinitive | No value |
| LDP10 | 28.5 | 28.5 | 28.5 | 1.98 | infinitive | No value |
| Fe | 7.6 | 7.6 | 7.6 | 1.9 | 20.09 | 10.6 |
| Uric acid | 16.2 | 15.9 | 16.05 | 3.5 | 29.6 | 8.4 |
| SHP | 5 | 5 | 5 | 0.0005 | 10508 | 21016000 |
| WBC | 6.1 | 6.1 | 6.1 | 0 | infinitive | No value |
| RBC | 35.7 | 35.7 | 35.7 | 23.8 | 115.7 | 4.9 |
| Hgb | 32.9 | 32.9 | 32.9 | 24 | 81.5 | 3.4 |
| Hct | 33.2 | 33.2 | 33.2 | 28.8 | 132 | 4.6 |
| Lymph Absol | 2.87 | 2.83 | 2.9 | 0 | infinitive | No value |

BMDexp and BMD hill are the two models applied in the PROAST program for calculations of the BMD. BMDlow and BMDhigh indicate the lower and upper end of the 90% confidence interval. The ratio calculated between the BMDlow and BMDhigh gives an indication of the range of the confidence  interval and the reliability of the data.

- BMD is presented in mg/kg of orally administered CuO NPs for 5 consecutive days. The bench mark dose (BMD) determination is performed at a 5% deviation of levels in vehicle control treated animals as bench mark.

- ALP05. The figure 05  indicates a deviation due to treatment compared to vehicle control with more than 5%. ALP10. Similarly for a deviation of more than 10%.

Supplementary Table 8  Bench mark dose calculations for effects after oral Cu2CO3(OH)2 NPs exposure for 5 consecutive days.

| Parameter | BMDexp | BMDhill | BMDavg | BMDlow | BMDhigh | ratio |
| --- | --- | --- | --- | --- | --- | --- |
| Day 6/7 |  |  |  |  |  |  |
| Body weight | 92.9a | 92.6 | 92.7 | 43.7 | 153.9 | 3.5 |
| Liver weight | 31.5 | 33 | 32.2 | 9.5 | 75.5 | 7.9 |
| Adrenal weight | 53.7 | 53.7 | 53.7 | 5.2 | 106.3 | 20.4 |
| Thymus weight | 69.6 | 68.5 | 69.1 | 43.1 | 97.2 | 2.3 |
| Spleen weight | 90.6 | 88.8 | 89.7 | 50.2 | 99.9 | 2.0 |
| AST | 30.7 | 30.9 | 30.8 | 18.8 | 42.9 | 2.3 |
| ALP05b | 94.1 | 88.8 | 91.5 | 65.6 | 95.6 | 1.5 |
| ALP10 | 101.1 | 95.7 | 98.4 | 75.2 | 102.8 | 1.4 |
| Fe | 101.5 | 101.5 | 101.5 | 34.9 | 122.7 | 3.5 |
| Uric acid | 90.5 | 90.5 | 90.5 | 36.1 | 93.7 | 2.6 |
| SHP | 97.0 | 93.1 | 95.1 | 77.6 | 100.8 | 1.3 |
| WBC | 27.6 | 27.1 | 27.4 | 0.9 | 55.4 | 56.8 |
| RBC | 108.6 | 108.7 | 108.6 | 70.8 | 112.5 | 1.6 |
| Hgb | 106.4 | 94.6 | 100.5 | 67.7 | 115.1 | 1.7 |
| Hct | 113.1 | 113.1 | 113.1 | 74.6 | 117.2 | 1.6 |
| Lymph rel | 96.5 | 92.3 | 94.4 | 65.2 | 97.9 | 1.5 |
| Lymph Absol | 101.0 | 98.4 | 99.7 | 45.4 | 106.1 | 2.3 |
| LDP05 | 61.8 | 61.8 | 61.8 | 32.2 | 91.1 | 2.8 |
| LDP10 | 70.3 | 70.3 | 70.3 | 41.2 | 97.9 | 2.4 |
| Day 26 |  |  |  |  |  |  |
| AST | 45.5 | 46.1 | 45.8 | 33.6 | 57.0 | 1.7 |

BMDexp and BMD hill are the two models applied in the PROAST program for calculations of the BMD. BMDlow and BMDhigh indicate the lower and upper end of the 90% confidence interval. The ratio calculated between the BMDlow and BMDhigh gives an indication of the range of the confidence  interval.

a) BMD is presented in mg/kg of orally administered Cu2CO3(OH)2 NPs for 5 consecutive days. The bench mark dose (BMD) determination is performed at a 5% deviation of levels in vehicle control treated animals as bench mark.

b) ALP05. The figure 05  indicates a deviation due to treatment compared to vehicle control with more than 5%. ALP10. Similarly for a deviation of more than 10%.