Supplementary information

Predominance Role of O2•− over •OH in the Dechlorination of TCE in Aqueous Phase using

Cu-TiO2

Landry BIYOGHE BI NDONGa(, Frank Herve YEO KANFOLOa

a College of Environmental Science and Engineering, Chang’an University, Xi’an, 710054, P.R.

China;

Table S1: Parameters values of TCE degradation using specifics scavengers at different solutions pH

| Experimental conditions | Degradation rate (%) | Pseudo first-order rate constant, k (min-1) | Correlation coefficient, R2 |
| --- | --- | --- | --- |
|  | pH 3 | pH 7 | pH 11 | pH 3 | pH 7 | pH 11 | pH 3 | pH 7 | pH 11 |
| UV alone | 64.71 | 52.54 | 56.10 | 0.0182 | 0.0120 | 0.0133 | 0.9881 | 0.9827 | 0.9697 |
| UV/TBA | 32.88 | 30.46 | 34.76 | 0.0064 | 0.0054 | 0.0072 | 0.9719 | 0.9130 | 0.9362 |
| UV/KI | 58.24 | 54.28 | 47.95 | 0.0148 | 0.0134 | 0.0118 | 0.9959 | 0.9971 | 0.9825 |
| UV/BQ | 13.00 | 16.41 | 10.95 | 0.0024 | 0.00.29 | 0.0019 | 0.9868 | 0.9024 | 0.9138 |
| UV/FA | 96.25 | 99.75 | 99.58 | 0.0195 | 0.0274 | 0.0201 | 0.7038 | 0.8073 | 0.7578 |
| UV/TiO2 | 100 | 100 | 100 | 0.1479 | 0.0959 | 0.0961 | 0.9994 | 0.9981 | 0.9698 |
| UV/TiO2/TBA | 38.34 | 38.29 | 17.75 | 0.0098 | 0.0098 | 0.0030 | 0.9131 | 0.9267 | 0.9168 |
| UV/TiO2/KI | 53.94 | 60.20 | 52.98 | 0.0143 | 0.0156 | 0.0128 | 0.9854 | 0.9792 | 0.9862 |
| UV/TiO2/BQ | 11.88 | 16.51 | 20.45 | 0.0020 | 0.0030 | 0.0038 | 0.9478 | 0.9581 | 0.8977 |
| UV/TiO2/FA | 14.85 | 25.14 | 27.36 | 0.0025 | 0.0040 | 0.0042 | 0.9140 | 0.9156 | 0.8597 |
| UV/Cu-TiO2 | 100 | 100 | 100 | 0.3380 | 0.2068 | 0.2554 | 0.9989 | 0.9970 | 0.9972 |
| UV/Cu-TiO2/TBA | 15.46 | 10.26 | 10.21 | 0.0028 | 0.0017 | 0.0015 | 0.8951 | 0.6718 | 0.6410 |
| UV/Cu-TiO2/KI | 51.12 | 64.67 | 48.17 | 0.0118 | 0.0163 | 0.0104 | 0.9819 | 0.9635 | 0.9714 |
| UV/Cu-TiO2/BQ | 21.64 | 19.09 | 39.40 | 0.0037 | 0.0034 | 0.0063 | 0.9758 | 0.7496 | 0.5892 |
| UV/Cu-TiO2/FA | 34.82 | 32.96 | 36.55 | 0.0065 | 0.0066 | 0.0075 | 0.9617 | 0.9887 | 0.9533 |

Figure S1 Comparisons of degradation and dechlorination rate of TCE over (a) UV alone and (b) UV/ TiO2

Figure S2 Stability test by TCE degradation in twenty cycles reuse of as-synthesized products

Figure S3 Effects of TBA, KI, BQ and FA on TCE degradation over UV alone in various solutions at (a) pH =3, (b) pH =7 and (c) pH =11

Figure S4 Effects of TBA, KI, BQ and FA on TCE degradation over UV/TiO2 in various solutions at (a) pH =3, (b) pH =7 and (c) pH =11

# Footnotes

( Corresponding author. Tel.: +86 29 82339052; Fax: +86 29 82339961.

E-mail address: biyoghendong@hotmail.com