Supplementary Material

## Supplementary Figures

Figure S1. TG and DTG curves of GB-derived biosilica.

Figure S2. FTIR spectra of biosilicas obtained from the different marine sponges.

## Supplementary Tables

Table S1. pH of DMEM before and after 3 days of incubation in the presence of biosilica particles

| Sample* | pH of DMEM |  |
| --- | --- | --- |
|  | before incubation | after 3d of incubation |
| GA | 8.1 | 8.8 |
| GB | 8.2 | 8.4 |
| SN | 8.2 | 8.5 |
| AI | 8.0 | 8.7 |
| PV | 7.9 | 8.2 |

* DMEM in the presence of the corresponding biosilica.

Table S2. ICP analysis of DMEM before (control) and after 3 day of incubation in the presence of biosilica particles

| Sample | Concentration, µg/mL |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Ca | K | Mg | Na | P | Al | Si |
| DMEM (control) | 116.142 ±0.041 | 300.385 ±0.173 | 31.559 ± 0.004 | 4042.528 ± 1.546 | 40.903 ± 0.065 | 0 | 7.486 ±0.004 |
| GA | 72.640 ± 0.008 | 312.753 ±0.110 | 34.760 ± 0.003 | 4181.305 ± 0.902 | 11.632 ± 0.069 | 0 | 112.780 ± 0.013 |
| GB | 77.808 ± 0.019 | 360.620 ±0.167 | 45.030 ± 0.008 | 4602.460 ± 0.186 | 39.053 ± 0.075 | 0 | 88.131 ± 0.037 |
| SN | 131.971 ± 0.046 | 480.614 ±0.206 | 54.131 ± 0.004 | 4741.862 ± 0.398 | 14.790 ± 0.006 | 0 | 86.900 ± 0.017 |
| AI | 86.211 ±0.019 | 332.393± 0.167 | 41.089 ±0.008 | 3943.505 ±0.186 | 29.459 ±0.075 | 0 | 73.867 ±0.037 |
| PV | 114.639 ±0.010 | 383.177 ±0.080 | 51.501 ± 0.004 | 4535.507 ± 0.967 | 23.490 ± 0.008 | 0 | 70.101 ± 0.008 |