

**S 1.** Dissolution profiles of PEL from SRSD (F6) at different pHs (Mean±SD, n=3).

**S2.** Release kinetic parameters of pelubiprofen in SRSD formulation

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Formulation | Zero order | |  | First order | |  | Higuchi model | | Hixson-Crowell | | |  | Korsmeyer-Peppas | | |
| r2 | k1 |  | r2 | k2 |  | r2 | k3 |  | r2 | k4 |  | r2 | k5 | n |
| SRSD (F6) | 0.7635 | 9.0136 |  | 0.9252 | 0.2151 |  | 0.9489 | 30.416 |  | 0.879 | 0.244 |  | 0.9451 | 38.3089 | 0.4274 |

r2, correlation coefficient;k1 – k5,constants of release kinetics; n, diffusional exponent



**S3.** IVIVC of SRSD (F6) formulation